A Multiscale thermomechanical METAL ADDITIVE MANUFACTURING simulation and the impact of geometry on residual stress and distortion

Luis Fernando Silva Velasco, M.S.

Western Michigan University, 2020

Metal additive manufacturing is an important technology, enabling the rapid prototyping and manufacturing of geometrically complex structures that would otherwise be difficult or impossible to manufacture. However, the manufacturing process can produce undesired residual stresses and distortions. The first part of work describes the implementation of a multiscale, transient thermo-mechanical simulation aimed at modeling the metal powder bed fusion additive manufacturing process to predict these residual fields. NASA’s Micromechanics Analysis Code was is to incorporate the microscale effects of an evolving material porosity on the predicted macroscale fields. The simulation shows that the evolving material porosity, as the material transitions from a metal powder to a solid, significantly affects the magnitude of the residual stresses and distortions, compared to a constant porosity model.

The second part of this work uses the developed simulations to assess the effects of geometrical features on these residual fields. A linear regression shows that there is some dependence of the residual fields on the geometry. This suggests that gaining some control of the residual fields may be possible through the geometry. This work is part of a larger study aimed at optimizing the geometry of a structure to minimize the residual stresses and distortions in a metal additively manufactured part.

A Multiscale thermomechanical METAL ADDITIVE MANUFACTURING simulation and the impact of geometry on residual stress and distortion

by

Luis Fernando Silva Velasco

A thesis submitted to the Graduate College

in partial fulfillment of the requirements

for the Degree of Master of Science

Department of Mechanical and Aerospace Engineering

Western Michigan University

May 2020

Thesis Committee:

Peter A. Gustafson, Ph.D., Chair

Jinseok Kim, Ph.D.

Pnina Ari-Gur, Ph.D.

© 2020 Luis Fernando Silva Velasco

ACKNOWLEDGEMENTS

I would like to first acknowledge and dedicate this to my parents Aureliano Silva Guerrero and Silvia Silva Velasco, who have sacrificed the unimaginable to guide me to this point in life, and to my extended family for their unconditional support. Furthermore, I would like to thank my advisor and friend Dr. Peter Gustafson who energetically pushed, pulled, opened doors, and unselfishly helped me throughout my graduate studies. Without a question this would not have been possible without his guidance. I would also like to thank and acknowledge all my past mentors and educators for putting me on this path in life.

This work was financially supported by a NASA Space Technology Research Fellowship, for which I am honored and thankful to have received. Immense gratitude is due to Dr. Evan J. Pineda for not only his technical assistance but also for the uplifting moral support in completing this project. I must also acknowledge several NASA personnel including but not limited to Brett Bednarcyk and Trenton Ricks for their technical support.

-Luis Fernando Silva Velasco

Table of Contents

1	Introduction	1

1.1	Motivation	1

1.2	Technical Problem	1

1.3	Technical Goals	3

2	Background and Literature Review	5

2.1	Metal Additive Manufacturing	5

2.1.1	Process	5

2.1.2	Post-Treatments	9

2.1.3	Experimental Measurements	10

2.2	AM Finite Element Simulation	11

2.2.1	The Thermomechanical FE Method	13

2.2.2	The Inherent Strain Method	20

2.2.3	Incremental Plasticity	23

2.3	The Generalized Method of Cells	27

3	Effects of an Evolving Porosity on Metal SLS	30

3.1	Implementation	31

3.1.1	Thermomechanical Set-up	31

3.1.2	Porosity and Material Properties	35

3.2	Results	42

3.2.1	Boundary Conditions	42

3.2.2	Evolving Porosity	45

3.2.3	Constant Porosity	49

3.3	Discussion and Conclusion	52

4	Effects of Geometry with Inherent Strain	55

4.1	Methodology and Implementation	55

4.2	Geometry and Validation	57

4.3	Results	60

4.4	Discussion and Conclusion	63

5	Geometry Effects with Thermomechanical FEA	64

5.1	Methodology and Implementation	64

5.2	Results	67

5.3	Discussion and Conclusion	76

6	Conclusion	79

7	References	82

8	Appendix	87

List of Figures

Figure 2.1 - Overview of laser-based powder bed metal AM.	6

Figure 2.2 - Simplified residual stress formation mechanism	7

Figure 2.3 - Plastic rheological analogy.	23

Figure 2.4 - A Doubly periodic RUC architecture, adapted from [24]	28

Figure 3.1 - Implementation flowchart, adapted from [26]	34

Figure 3.2 - Changing porosity	38

Figure 3.3 - Triply periodic open-cell RUC	39

Figure 3.4 - Sintered material homogenized macroscopic stress-strain curve.	40

Figure 3.5 - Elastic modulus vs. temperature vs. volume fraction.	42

Figure 3.6 - Geometry and mesh used.	44

Figure 3.7 - Boundary conditions applied.	44

Figure 3.8 - Laser beam scanning path.	45

Figure 3.9 - Results at t = 31.5s, evolving porosity, no deformation shown.	46

Figure 3.10 - Results at the end of print, t = 72s, deformation magnified by 20x, evolving porosity.	47

Figure 3.11 - Estimated porosity vs. time, at node point C.	48

Figure 3.12 - Results at t = 31.5s, constant porosity, no deformation shown.	50

Figure 3.13 - Results at the end of print, t = 72s, deformation magnified by 20x, constant porosity.	51

Figure 3.14 - Von Mises stress, at t=72s, deformation magnified by 20x	52

Figure 3.15 - Equivalent plastic strain, at t=72s, deformation magnified by 20x.	53

Figure 4.1 - Geometry of 10 mm cube, Ø 5 mm, 5 mm blind hole	57

Figure 4.2 - Inherent Strain and thermomechanical comparison, 8 mm diameter, deformation magnified 20x	59

Figure 4.3 - Cantilever beam deformation, before (top) and after (bottom) stress release, no deformation magnification	59

Figure 4.4 - Von Mises stress of geometry with various hole diameter, deformation magnified 20x	62

Figure 4.5 - Hole diameter effects, inherent strain	62

Figure 5.1 - Preliminary cantilevered beam simulation	67

Figure 5.2 - Geometry and varied parameters	67

Figure 5.3 - Sampled LHS inputs	68

Figure 5.4 - Representative mesh and laser scan pattern, specimen #1	68

Figure 5.5 - Representative von Mises stress plots, before (left) and after (right) stress relieving, deformation magnified by 100x, specimen #1	69

Figure 5.6 - Representative von Mises stress plots, before (left) and after (right) stress relieving, deformation magnified by 100x, specimen #1	70

Figure 5.7 - Representative stress plots, before (left) and after (right) stress relieving, deformation magnified by 100x, specimen #1	70

Figure 5.8 - Solution at the end of print, before removing from bed	72

Figure 5.9 - Solution at the end of print, after removing from bed	73

Figure 5.10 - Quadratic regression fitted plots, before stress release	75

Figure 5.11 - Quadratic regression fitted plot, after stress release	76

Figure 5.12 - Representative porosity, no deformation shown, specimen #1	78

List of Tables

Table 3-1 - Solid Inconel 625 properties used as a function of temperature	40

Table 3-2 - Laser parameters	45

Table 3-3 - Residual stress and distortion comparison.	52

Table 4-1 - Inherent strain, geometrical feature  results	60

Table 5-1 - Sampled LHS inputs	68

Table 5-2 - Linear regression results; partial table; MPa - mm units	74

Table 8-1 - Porous material properties computed with NASA’s MAC/GMC from Table 3-1	88

Table 8-2 – Continuation of Table 8-1	89

Table 8-3 - Linear regression results, Chapter 5, MPa - mm units	90

Table 8-4 - Quadratic regression results, Chapter 5, MPa - mm units	91

List of Abbreviations

ε	=	sintered porosity, strain

ε0	=	initial porosity

εmin	=	minimum achievable porosity

K	=	densification coefficient

κ	=	sintering coefficient

Vf	=	volume fraction

s	=	laser beam penetration depth

η	=	laser power transmission efficiency

r0	=	laser beam radius

v	=	laser linear speed

l,w	=	length and width of the laser scan area

ψ	=	specific energy input

P	=	nominal laser power

Sxx	=	stress in xx-direction

Sy,Sn	=	yield stress, stress at plastic strain n

σ,  σ	=	stress tensor, stress tensor Vioglot representation

H	=	strain hardening term

Ui	=	displacement in the i-direction

ε*	=	inherent strain

υ	=	Poisson’s ratio

E	=	modulus of elasticity

Q	=	heat per unit volume

qb	=	heat flux at a boundary

c	=	specific heat capacity

ρ	=	mass density

k	=	thermal conductivity

h	=	convective heat transfer coefficient

σ	=	Stefan-Boltzmann constant

C	=	specific heat capacity

α	=	coefficient of thermal expansion

T	=	Temperature

B	=	deformation matrix

D	=	constitutive matrix

N	=	shape function matrix

κ	=	thermal conductivity matrix

K	=	stiffness matrix

τ	=	out of plane thickness, shear stress

List of Acronyms

AM – Additive Manufacturing

DED – Direct Energy Deposition

DOF – Degree of Freedom

EBM – Electron Beam Melting

FDM – Fused Deposition Modeling

FE – Finite Element

GMC – Generalized Method of Cells

HIP – Hot Isostatic Pressing

ICME – Integrated Computational Materials Engineering

ISM – Inherent Strain Method

MAC – Micromechanics Analysis Code

NASA – National Aeronautics and Space Administration

PBF – Powder Bed Fusion

RS – Residual stress

RUC – Repeating Unit Cell

SIMP – Solid Isotropic Material with Penalization

SLS – Selective Laser Sintering

SLM – Selective Laser Melting

TGM – Temperature gradient mechanism

CHAPTER 1

# Introduction

## Motivation

Advancements in metal additive manufacturing (AM) have made it a viable solution for the rapid prototyping and manufacturing of geometrically complex parts. These complex parts can be difficult or impossible to manufacture with conventional subtractive manufacturing. However, the additive manufacturing can be accompanied by large residual stresses. These stresses can lead to premature failure due to crack promotion or otherwise weaken the overall structure [1]. In addition, the part deformation that occurs in conjunction with the residual stresses may cause unacceptable dimensional deviations. Although several post-treatment processes exist to mitigate these negative outcomes, the permanent deformation caused by plastic strain is not easily reversed.

## Technical Problem

The prediction and reduction of these residual fields is desirable. Although residual stresses and plastic deformations occurs at the local scale, it may be possible to mitigate the negative effects of additive manufacturing by modifying the macroscopic geometry. The larger project aims to obtain an optimized the geometry to minimize the residual fields, without adversely affecting the final application. Since it is common that AM parts are already geometrically optimized for its final application, a multi-objective technique is required. This requires an objective function that accounts for the manufacturing process, not just the final application of the part. The geometrical optimization is a component of the larger project and is outside the scope of this thesis work.

The first element in achieving the overall goal is to obtain a computer simulation of the manufacturing process. This is needed to compute the value of the manufacturing component of the objective function. Simulation of this additive manufacturing process is intrinsically difficult since the domain of interest occurs at the nano and micro scale, while the structures being simulated are in the macroscale domain. This requires a multiscale solution. Also, the manufacturing process involves multiple physics, with the melting requiring thermo-fluid-dynamics, the material deposition and microstructural evolution requiring methods accounting for phase transformations, and resolution of the stress-strain fields requiring conventional mechanics at the macroscale. In addition, due to the addition of thin layers of material, the manufacturing process can be composed of thousands of steps each with different and moving boundary condition, requiring a substantial number of time steps during the simulation. Due to these difficulties, many techniques have been used in the literature that drastically reduce the size of the problem by making several assumptions, such thermomechanical method where melt pool dynamics are not considered, and the inherent strain method, where the dynamic heat transfer physics are not considered.

## Technical Goals

The first goal of this work is to simulate the metal powder bed fusion additive manufacturing process. As a sub-goal, the micromechanics of the simulation can be considered using the available tools from NASA. This can be used to study the effect of the micromechanics on the thermomechanical simulation. Specifically, the material’s evolving porosity (the air to solid volume fraction), changing from powder to solid, was chosen as the microscale variable of interest. To the authors knowledge, the effect of an evolving porosity on the predicted residual stresses and distortions has not been investigated. In addition, this work lays the foundation to analyze other microscale effects on the macroscale. The inclusion of the micromechanics and its effects onto the macroscale mechanics during the simulation of the manufacturing process is a step in the implementation of an Integrated Computational Materials Engineering (ICME) method on metal additive manufacturing.  Work in ICME aims to using computer simulations to design and engineer not only the final products but also their constitutive materials. This requires multiscale methods to simulate the evolving material properties during manufacturing. This first goal is achieved in Chapter 3 Effects of an Evolving Porosity.

The second goal of this work is to test if the geometry can influence the simulated residual stress and deformations acquired during manufacturing, and if so how. This will assess the feasibility of the long-term goal of obtaining a geometry optimized for its manufacturing process. This feasibility study requires the tools developed for modeling multiscale effects such as porosity. This goal of assessing geometric effects is achieved and discussed in Chapter 4 - Effects of Geometry with Inherent Strain and also in Chapter 5 - Effects of Geometry with Thermomechanical FE.

CHAPTER 2

# Background and Literature Review

## Metal Additive Manufacturing

### Process

Metal additive manufacturing processes include powder bed fusion (PBF) and direct energy deposition (DED) process. Powder bed fusion processes include selective laser melting (SLM), and electron beam melting (EBM). These use a high-powered energy source (a laser or electron beam) to selectively melt or sinter sections of metal powder into a solid, a layer at a time [2]. A recoating mechanism ensures that a uniform layer of powder is added to the powder bed at each layer. An inert gas environment is used to contain the powder bed in a laser-based process, while electron beam melting uses a vacuum. Figure 2.1 shows an overall schematic of the powder bed fusion laser process.

The powder layers are relatively thin compared to the part size, typically 30-50μm for lasers, around 100μm for electron beams [2], thus requiring potentially thousands of layers to build up the geometry. In addition, the powder bed fusion process will re-melt the underlying layer as the topmost layer is being melted. Direct energy deposition methods, in contrast to powder bed fusion, feed the material onto the part as it is being melted. The feedstock material is a metal powder or wire. Direct energy deposition methods typically have faster print times at the sacrifice of lower dimensional accuracy [2].

Metal

Powder

Recoater

Part

Inert gas environment

Laser

Figure 2.1 - Overview of laser-based powder bed metal AM.

However, these manufacturing processes can suffer from significant residual stresses, stresses that may lead to unacceptable part distortion and that promote cracks, adversely affecting the life of the part [3]. Large distortions may also cause damage to the recoater system in PBF processes. Residual stresses arise primarily due to the large temperature gradients during the process. The temperature gradient mechanism (TGM) model reasons that the thermal expansion during heating causes stresses on the underlying already solidified material [4]. Plastic strains may develop here due to the thermal loading. During cooling, the shrinking material induces tensile and compressive stresses on the surrounding material. However, in practice, the complicated thermal history produces complex stress distributions [4]. Thus, the field strongly depends on all the factors affecting the temperature history, such as beam path, and dwell time. Figure 2.2 shows a simplified overview of the temperature gradient mechanism.

εplastic

σcompressive

σtensile

Heating

Cooling

σcompressive

Figure 2.2 - Simplified residual stress formation mechanism

During the mechanical loading of the material, large changes in stress occur, characterized by three phases. Phase one has large temperature changes, phase two has large stress changes (tensile to compressive) and phase three results in the steady-state residual stress after creep relaxation [5]. Three types of residual stresses exist on three different scales: macroscale, microscale, and nanoscale [4]. However, micro- and nano- scale stresses have limited effects on the overall mechanical properties [4]. Microscale stresses arise from anisotropic effects of the material, while nanoscale stresses arise from coherency and dislocations [4]. Experimental data shows that typically compressive stresses arise towards the center of the part, while tensile stress form at the outer surfaces of the material [6]. It is these tensile stresses that are detrimental to the fatigue life of the part.

Mercelis et al. in [2] have shown that the residual stresses in metal additive manufacturing  methods such as selective laser sintering (SLS) and selective laser melting (SLM) are significant,  predicting stresses as high as 700 MPa in Inconel 718. Li et al. in Ref. [4] cite residual stresses at 50% to 60% above the materials yield strength. They also found that the manufacturing process parameters such as the beam size, power and scanning speed affect the magnitude of the produced residual stresses, thus in-process methods exist to reduce these residual stresses.

In-process stress mitigation methods include closed-loop feedback control (controlling the heat source, aiming to homogenize the temperature distribution), thermal gradient control (preheating the ambient to reduce thermal gradients), scanning strategy control and mechanical control (laser shock peening) [4]. A scanning strategy in a chessboard pattern has been shown to cause less distortion than other scanning strategies [4].

In addition, AM parts show a columnar microstructure in the build direction in nickel-based superalloys, titanium alloys and stainless steels [4]. This alludes to the anisotropic mechanical properties seen in parts [7]. Thus, it is worthwhile to investigate the effects of the microstructure on the residual fields.

### Post-Treatments

After manufacturing, heat treatment processes such as hot isostatic pressing (HIP) have significant benefits to the mechanical characteristics of a part. During HIPing parts are subjected to high temperatures and high pressures (1120 - 1240 °C, 100 - 165 MPa) for several hours (3 - 4 hr.) in an inert environment [8]. This treatment can significantly reduce the residual stresses, reduce the internal porosity and defects, and decrease the anisotropy of the material’s properties [8]. Reference [9] showed that the HIPing of an metal additively manufactured beam specimen reduced the residual stresses up to 70%. In addition, HIPing of an SLM produced part can significantly increase its fatigue characteristics, due to the internal closing of pores, with further improvements when the surface of the part is conditioned (i.e. polished or machined) [10]. Other mechanical post-processing such as hard turning, shot peening, and grinding can generate potentially advantageous compressive stresses on the surface and subsurface [4]. Also, post-treatments can dramatically reduce the dislocation density, signifying a reduction of microscale residual stresses.  Although post-processing can remove elastic deformations acquired during the manufacturing, they cannot remove plastic strains/deformations. Thus, additional processing is required such as machining. Processing that increases the manufacturing costs.

### Experimental Measurements

Several experimental methods exist to measure residual stresses depending on the scale of the stress [11]. Mechanical methods rely on relaxing the residual stress in the part with a machining procedure. The deformation after the machining operation then is used to calculate the residual stress before the operation [11]. These methods are used to measure macroscale stresses (those that vary continuously over large scales). In the curvature method, the stressed part is sectioned into narrow strips (to avoid multiaxial stresses) and the deformation/curvature of the part after the stress relief is measured, with strain gauges for example. The stress can then be calculated from the material properties [11]. The hole drilling technique is typically a cheap method to obtain an approximate measurement. Here, the stresses can be inferred from measurements of a rosette of strain gauges [11] after drilling a hole.

Similarly, a method often used in the literature [12] is to additively manufacture a cantilever beam. Removing this part from its substrate will cause the beam to deform. The amount of deformation can then be measured. The stress required to obtain that deformation can then be calculated (theoretically or experimentally).

Diffraction techniques use the measured interplanar spacing to calculate the elastic strain [11] and thus the stress. Note that this requires a stress-free interplanar spacing as a reference. X-ray diffraction has a penetration in the order of micrometers (thus limited to surface measurements) while electron diffraction can only be used with very thin samples [11]. Other methods also exist, such as ultrasonics, where the change in speed of sound in the material can be used to calculate the average stress along the wave path [11].

## AM Finite Element Simulation

The AM process has been simulated in the literature using several methods. These include thermomechanical simulations with the finite element method (FEM), thermo-fluid simulations with the finite volume method, inherent strain methods with FE methods, microscale lattice Boltzmann methods, phase-field modeling, and microscale hybrid methods [3]. This work is concerned with the thermomechanical finite element method.

The temperature distribution of a moving point heat source can be approximated analytically by the Rosenthal solution [13]. The solution for a thick plate is shown in Eq. , where T0 is the ambient temperature, P is the heat power absorbed into the material, v is the heat source velocity in the positive x-direction, and α, k are the materials thermal diffusivity and conductivity respectively. However, the solution does not account for nonlinearities such as melt pool dynamics. In addition, this analytical solution also assumes constant material properties and neglects any latent heat. These shortcomings necessitate numerical solutions over the analytical solution in Eq. . In numerical simulations of the process, simulations that do not include temperature dependent material properties usually lead to inaccurate results [3].

A major disadvantage with FE methods is that with large models, especially with nonlinearities included, are computationally costly. In addition, the thermomechanical finite element method does not lend itself to easily include other physics in the simulation such as melt pool thermo-fluid dynamics [3], and metal evaporation [14]. Neglecting these physics can lead to inaccurate results when simulating large scale models [3], since the temperature distribution and gradients are the driving force in deformation and residual stresses. However, the fluid dynamics in FEM have been considered, approximating these physics by adjusting the thermal properties [15]. Thermo-fluid dynamics models have been conducted [16] (using an electron beam as the heat source) that includes fluid viscous effects, and phase transformations. Ref. [17] used lattice Boltzmann method which included capillary and wetting effects to simulate the melt pool dynamics to predict defects.

### The Thermomechanical FE Method

An uncoupled thermomechanical simulation is a two-step simulation, where first a transient thermal field is solved. The temperature distribution is then used in a quasi-static mechanical simulation as the loading. A quasi-static mechanical solution is used since the wave propagation speed of a mechanical transient problem for typical materials is orders of magnitude higher than the wave propagation speed of a thermal transient problem. Thus, it is assumed that mechanical problem is in quasi-steady state relative to the transient thermal problem.

For completeness, a condensed overview of the derivation of the thermal finite element method is shown here. For details the reader is referred to Cook [18]. The governing differential equation for the two dimensional heat transfer problem is shown in Eq. , where τ is the out of plane thickness; the three dimensional version is similar. Note that in this document, vectors are denoted by an underline while matrices are denoted by a boldface typeset, and a comma after a variable indicates a partial derivative.

Using the definitions shown in Eq. , where l, m, n are the direction cosines, the general three dimensional governing differential equation can be succinctly written as shown in Eq. , where κ is a matrix of thermal conductivity (in the global coordinate system) and Q represents heat generation rate. Essential (on temperature) and nonessential (on heat fluxes qb) boundary conditions can then be applied on this equation. For the two-dimensional problem, the boundary heat flux due to convection is, qb=hT∞-T. The boundary heat flux due to radiation is qb=ησTf4-T4, where η is the absorption value, and σ is the Stefan-Boltzmann constant, note that T must be in absolute units.

The functional to be minimized for the 2D problem can then be written as shown in Eq. , adding the convective boundary condition that is normal to the 2D plane. Discretizing the domain using the finite element method as shown in Eqs. , the functional can then be written as shown in Eq  for a single element, where definitions are as shown in Eqs. .

After assembling into global matrices (denoted by capitals) and making the functional stationary δΠδT=0 leads to Eqs.  from [18]. This equation can then be integrated though time numerically to obtain the solution. Note that the thermal problem does not have second time derivatives on temperature.

Once the temperature at a time step is found, it can be applied as a load to the static structural problem. Typically, the same mesh and element type that was used for the thermal problem is used for the mechanical problem, thus temperatures are already known at the nodes. If a different mesh is used, the temperature can simply be interpolated onto the new mesh using the shape functions of each mesh. The temperature change (from a reference point) is used to compute the thermal strains from the given vector of thermal expansion coefficients, as shown in Eqs. , dimensions of the vectors are shown for convenience.

The loading caused by this initial thermal strain must be applied on the right hand side of the static mechanical FE Eq. . This thermal force is computed from Eq. , where D is the constitutive matrix. In post processing, the thermal strain is then subtracted from the computed mechanical strain to compute the stress, Eq. . This process ensures that when a temperature change is applied to an unrestricted structure, the structure will deform, yet no stress will be present and vice-versa, as expected.

The uncoupled thermomechanical method is a one-way method, that is the mechanical simulation does not influence the thermal simulation. In coupled thermomechanical method, the thermal and mechanical problems are solved simultaneously, thus allowing for heat generation due to strains (such as plastic strain) to be included in the thermal simulation. For the work presented in this thesis (described in chapter 3 - Effects of an Evolving Porosity on page 33), the uncoupled method was used, assuming heat generation from plastic strain rates are negligible.

To resolve the continuously changing geometry, element “birth and death” (activation and deactivation), “quiet” elements, and a combination of these two methods are used in literature [19]. For the element birth and death technique, in first step of the simulation, all the elements are deactivated, that is they are not included in the solution (more specifically in KU=F . Element layers are then activated in subsequent steps, as the heat source is passed over the elements, until a fully completed part. The advantage of this method is that the model has a relatively small number of degrees of freedom (DOF) at the start and more DOF are added as the simulation progresses. The quiet element technique is similar; however, all of the elements are included in the solution, and elements that are yet to be included in the solid geometry are assigned material properties a several orders of magnitude smaller than the solid material properties. Nonzero material properties are assigned to avoid numerical difficulties. The hybrid method is a combination of these two methods. In this method, a whole layer of elements is activated (included in the solution) while elements where the laser has not yet passed over are assigned powder or weak material properties.

As described in section, 2.1 - Metal Additive Manufacturing on page 5, a typical layer thickness during manufacturing is in the order of 30 - 100 μm. In addition, the laser diameter is also in the order of 100 μm. Very high thermal gradients results from a small laser diameter [14]. It is impracticable to have a mesh density that is fine enough to resolve these features when a full-scale model is being simulated. Thus, it is typical to cluster many printed layers into a single layer (a superlayer) of elements during the FE simulation [20], along with an element density on the printing plane that does not capture such a high thermal gradients. Typically during a simulation at the macroscale (part sized) the laser diameter is set to a value much larger than reality [21]. The lumping of printed layers onto a single or a couple element layers can be justified by considering that the laser path is typically rotated at every printed layer, thus the effect of the detailed laser raster pattern is averaged out over several layers [20]. In addition, Ref [22] studied the effect of lumping many printed layers in to an equivalent superlayer of elements. Results show that the lumping can drastically reduce the number of DOF in the models with a small accuracy penalty, comparing simulation to experimental results. However, the size of the equivalent layer (i.e. number of printed layers in the element layer) should not be done arbitrarily, as the error increases as more printed layers are lumped [22].

In simulating the additive manufacturing process, nonlinearities in both thermal and mechanical problems exist, mainly nonlinearities in the heat input (the heat input is a function of time) for the thermal problem, plasticity in the mechanical problem (residual stresses arise due to plasticity) and temperature and time dependent material properties in both problems. Thus, an iterative solution is required for both problems. If the mechanical solver requires a smaller time step (to obtain a smoother load input for convergence), the thermal problem must be solved again at that new time step. Thus, the time step size is typically limited by the mechanical problem. It is evident that the thermomechanical method requires considerable computational power to simulate the entire manufacturing process, especially for large models.

To mitigate these computational inefficiencies, other methods have been utilized in literature. These methods include mesh coarsening, where the current  topmost layer uses a high-density mesh is used to resolve the solution in the heat affected zone, while a coarse mesh is used in areas far from the zone [21]. Thus, it is possible that growing the geometry (from the addition of material) does not lead to more nodes in the finite element problem. Since the heat affected zone is moving with respect to time as new layers of material are deposited, the model must be re-meshed. The solution is interpolated at every mesh change to a master fine mesh for postprocessing.

Other methods to reduce the problem size to allow the simulation of large models include the equivalent scanning method [3]. The equivalent scanning method applies a representative surface heat flux to a target volume or to an entire layer at a time [3], instead of modeling the laser path at every time step in the thermomechanical simulation. Another method used is the inherent strain method (ISM).

### The Inherent Strain Method

The inherent strain method (ISM) drastically reduces the problem size by avoiding the thermal simulation, and directly applying any irreversible strains as an initial strain in the mechanical problem. Temperature dependent properties are not needed since properties at room temperature are used [3]. These inherent strains include the residual plastic, creep, and phase transformation strains produced by the thermal loading and unloading. ISM relies on the assumption that small patches of material all experience a similar thermo-mechanical history, thus no need to model a moving heat source, as the irreversible strain produced by the heat source is directly applied to the mechanical problem [3]. This assumption is reasonable considering that the laser scanning pattern is repetitive. The inherent strain method was initially conceived for the computation of welding mechanics. The metal AM process is in a sense a continuous welding process, hence application of the inherent strain method on the additive manufacturing process. Eq.  provides the definition of inherent strain [22]. Since the inherent strain is applied to the static mechanical simulation, the part has had enough time to cool, thus thermal strains are neglected. Furthermore, strains due to phase transformations and creep are typically neglected, thus the inherent strain is approximately only the plastic strain [22].

However, the assumption that this strain is the same everywhere is not accurate for the AM process as it is for its original intended usage, a welding process [22]. The strain produced is dependent on the boundary conditions and thermal boundaries, which are changing in AM, thus this method may be inaccurate for complex parts, or parts for which the inherent strain applied has not been calibrated. In addition, the method assumes the same strain for all the layers, however, in AM, the inherent strain from the layers above could change the plastic strain of the layers below. It has also been shown [12] that this inherent strain is highly dependent on laser scanning pattern and orientation. Reference [22]  states that the inherent strains decrease sharply near the ends of the layers due to differences in the thermal and mechanical boundary conditions.

Eq.  shows how this strain is applied to the static FE mechanical problem, noting that this equation is equivalent to Eq. . That is the inherent strain is treated as an initial strain (equivalent to an initial thermal strain). Eq.  through Eq.  show how the mechanical problem conventionally solved in the finite element method. This strain is applied to a whole element layer at a time [22]. In addition, since the laser pattern is rotated at every printed layer, it is usually assumed that the inherent strains in the print plane are equal (i.e. ε*xx=ε*yy). This is assumed since the lumped element layer represents many printed layers, thus the in-plane strains are averaged out, since the laser scan pattern is rotated at every layer.

During simulation, like the thermomechanical method, element activation and deactivation is used to activate a layer of elements representing several AM layers. Then the inherent strain is applied to the whole layer of elements at a time. This in addition to avoiding the thermal simulation aids in the computational time.

The specific inherent strain is either experimentally determined or found with a high-fidelity thermomechanical FEM simulation on a small representative volume. Only normal components of the inherent strain tensor are considered as these are the dominant strains [12]. This inherent strain can be experimentally obtained [12] by simply applying an estimated strain onto a model using this method to predict a distortion on a part. This part can then be manufactured, and the distortion measured. The simulation can then be iterated with a different inherent strain until the model agrees with the experimental measurements. A root finding numerical algorithm can be used to iterate through the simulation.

It has been shown that the laser path (and thus the temperature distribution) affects the effective inherent strain [12]. A major disadvantage of the inherent strain method is that calibration of the applied inherent strain may lead to accurate results for one geometry; however, it may predict inaccurate results with other geometries [3].

### Incremental Plasticity

For completeness, a brief summary of incremental plasticity is given here, since it is plasticity that is responsible for the accumulation of residual stresses in part after the loading has been removed. This section is a review of reference [23]. The analogous rheological model commonly used (ref here) to illustrate the concepts of plasticity is given in Figure 2.3.

F

M

Figure 2.3 - Plastic rheological analogy.

The yield criterion provides a threshold for the onset of plasticity for a given loading and internal material parameters (history dependent). The yield criterion is shown in Eq. , where σ represents the stress tensor, and α are internal state parameters. Positive values for this function are inadmissible, values less than zero represent an elastic state, while a state at the boundary f=0 represents a plastic state of stress. With a perfectly plastic model (no hardening) the stresses in the stress tensor must be redistributed around the yield surface (represented by f=0 ) if the loading is to be plastic.

It is typical that the von Mises criteria is used as the yield criteria. Using this the yield criterial can be written as shown in Eq. . Note that the yield stress σ0(α) is not a constant, as it is loading history dependent due to material hardening. Since any stress state where the yield function is greater than zero is not possible, this implies that any loading/unloading (i.e. a stress increment dσ) must stay on the surface, implying df≤0, named the consistency equation, where a df<0 represents an unloading condition. For a perfectly plastic material (no hardening), this can be written as in Eq. , where ∇f  is defined as ∇fT=δfδσxx⋯δfδτzx .

df=∇fT∙dσ≤0

The increment in plasticity is assumed to be decomposed of an increment in elastic strain and an increment in plastic strain as shown in Eq. . An increase in plastic strain is then assumed to be normal to the gradient of the yield function (the associative rule) as shown in Eq. .

Then the incremental stress strain relationship is written as in Eq.

Substituting Eq.  into the consistency equation and solving for dλ gives Eq. .

Then substituting back into the incremental stress-strain relationship Eq.  and solving for Dep gives Eq. , noting that D is a square matrix.

To include hardening effects, a uniaxial stress-strain curve (piecewise linear) is used to calculate a hardening term H. Since the stress-strain curve (typically obtained experimentally) is locally linear the hardening term can be calculated as shown in Eq. . Note, E1 and E2are the slopes of the curve at two different points.

For isotropic hardening the yield surface grows equally in all directions in the principle stress space, this implies dσdεp,eq=dσ0dεp,eq=H. Thus, σ0εp,eq=H⋅dεp,eq, and again H can easily be calculated from the stress-strain curve as shown in Eq. . Thus, σ0(α)=σ0(εp,eq), where the equivalent plastic strain is found similarly to the von Mises stress formulation. This also implies that dεp,eq=dλ from the solution of dλ in Eq. . Then the consistency equation can then be written as Eq. , where the second half assumes isotropic hardening. Thus, the incremental plasticity constitutive matrix is shown in Eq.  found using a similar derivation as above. Note that Eq.  is nonlinear, thus requires an iterative numerical algorithm to solve, typically a modified version of Newton-Raphson is used. Return algorithms are also used to ensure that the yield criterion is always satisfied (i.e. f≤0) when solving the equations numerically. In the finite element method, the tangent stiffness matrix is defined similarly as its linear version (K=ΩBT⋅D⋅BdΩ) however, with D replaced by Dep.

## The Generalized Method of Cells

This work makes use of NASA’s Micromechanics Analysis Code MAC) which implements the generalized method of Cells (GMC) MAC/GMC. A brief review is included here for background. The generalized method of cells uses a Repeating Unit Cell (RUC) to represent the microstructural domain of heterogeneous material [24]. This section provides a brief description of GMC as described in Aboudi [24]. Each repeating unit cell then contains sub-cells that are representative of distinct phases or distinct materials in a composite, in this case, neighboring metal particles and trapped air in the metal powder during the sintering process. This is shown in Figure 2.4. The material properties and dimensions of each sub-cell can then be used to compute the effective homogenized macroscopic response (stress/strain, thermal/mechanical material properties) of the repeating unit cell [24]. These effective material properties are used as the constitutive model in the FE simulation, effectively cascading the microstructural response onto the macroscale.

Matrix

Matrix

Matrix

Fiber

Figure 2.4 - A Doubly periodic RUC architecture, adapted from [24]

The method of cells assumes the displacement of every subcell (denoted by   α,β,γ) is linear. For a doubly periodic subcell this can be written as shown in Eq. . Note that the origin of the xi frame is at the center of each subcell. This equation introduces several micro-variables ϕiβγ,Ψiβγfor every subcell. These can be solved for by enforcing continuous displacements at every subcell interface and with adjacent unit cells. This is done in an average sense, that is as shown in Eq. . The subcell strains and stresses can then then be found from elastic theory. The cell’s homogenized stress and strain is then the volume averaged of every subcell. Note that the total strain (and therefor the stress) is constant in every subcell. Then subcell traction continuity is also enforced at the interfaces. This gives sufficient equations to solve for all the micro-variables, thus the subcell’s constitutive relationship can be found. Using the volume average strains the RUC’s homogenized constitutive relationship can be found as shown in Eq. , where bij is found from the micro-variables (by solving a system of equations) and the subcell’s geometry. In addition, for a given macroscopic state, the state of all the subcells can be found using a localization matrix. For more details, the interested reader is referred to [24].

The generalized method of cells can incorporate the complex multi-scaled nonlinear material analysis and account for the coupling between thermal, strain, plasticity, and multi-phase effects. The GMC generalized method of cells has the advantage that it can capture the phenomena more natively  at the microscale, as opposed to other microstructural to macrostructural estimates, such as the Voigt approximation or the Reuss approximation [24, p. 105].

CHAPTER 3

# Effects of an Evolving Porosity on Metal SLS

This chapter describes the work conducted by Silva et al. in source [26]. To the authors’ knowledge the effect of porosity on the material properties (and consequently on the final residual stresses) have not been studied. This paper investigates the effect of modeling the evolving material properties based on the predicted porosity in-tandem with the conventional time-dependent thermomechanical AM simulation. The goal of this chapter is not to present validated results, but to show that material evolution (specifically porosity) can have a significant effect on the large-scale residual stresses and distortions.

A regression model from source [14] was used to predict the material porosity from the applied laser characteristics, laser diameter, power, and velocity. The porosity is then used as input to predict the homogenized macroscale material properties. Properties of Inconel 625 were used as the pristine material properties. To aid in computational speed, these material properties were precomputed for a range of volume fractions (porosity) and a range of temperatures, using NASA’s Micromechanics Analysis Code with the Generalized Method of Cells (MAC-GMC). This is used to compute the elastic modulus, Poisson’s ratio, thermal conductivity, specific heat capacity, coefficient of thermal expansion, and the plastic stress-strain response (pointwise incremental plasticity).

As a comparison, the simulation was conducted with material porosity kept at a constant, simulating a homogeneous material. A comparison with a homogenous model and the evolving model shows that the evolving porous model predicts larger distortions with greater residual stresses.

## Implementation

### Thermomechanical Set-up

Details of the thermomechanical method is given in section 2.2 AM Finite Element Simulation on page 11. The nonlinearity from the temperature-dependent material properties, the temperature-dependent plasticity model, radiation effects in the thermal model, and the changing materials from powder to solid require an iterative solution at every time step. Modeling of liquid phases, the latent heat of a solid to liquid phase change, and any creep effects are neglected. The open-source FE software CalculiX was used to perform the simulations.  Access to the source code permitted a highly configurable simulation.

External thermal loading was accomplished through a user-defined subroutine in CalculiX. This allows for controlled laser properties such as its path, intensity, and applied heat flux distribution. It has been shown that the laser scanning pattern influences the residual stresses of the final part [27]. Thus, the open-source 3D slicer software, Slic3r, was used to generate g-code describing the laser path of the part. The laser path produced by Slic3r is intended for a fused deposition modeling (FDM) 3D printing process. However, it was deemed the path produced was appropriate for the intent of this application, since the software is highly configurable and can be set-up with various laser scanning strategies.

A script was written to parse the g-code. It estimates the time required to perform each g-code operation from the laser speed. The script then interpolates the position of the laser at regular time intervals to populate a tabulated file. This file was then read by the user-defined subroutine (DFLUX) during the runtime in CalculiX.

The user subroutine reads the file and applies a Gaussian distributed volumetric heat flux  as computed by Eq.  from Ref. [28] to the corresponding integration points, at the current simulation time, simulating the laser energy input [25]. Note that, the expression π1-expKzs is a unitless constant in this model at approximately -59.959. The variables x and y are the distances from the beam’s center in the respective directions to the integration point, and z is the distance from the top surface to the integration point. The laser center is moved in steps, as described by the tabulated file. It is important that the file is only read once on the first call to the subroutine. This was implemented using the SAVE keyword in Fortran to keep the tabulated data in memory between subroutine calls.

Element activation simulates the addition of material deposited at every layer. A deactivated element is not computed as part of the solver pass. This method is described in section 2.2 - AM Finite Element Simulation on page 11. Each layer of elements represents several layers of the AM process, as the thickness of an FE element is substantially larger than the thickness of a powder layer. The element thickness for this work was chosen at 1 mm for ease of computation and proof of concept. Justification of this approximation is discussed in section 2.2 - AM Finite Element Simulation on page 11. A new layer of elements is added after the laser has finished passing through the previous layer. During the activation, since the layer below the newly added elements has already been strained, artificial strain is added to the newly activated elements. This ensures that the newly added, yet deformed element is stress-free.

Another python script performs the sectioning of a predetermined FE mesh into sets of element layers during preprocessing. After reading the input mesh file, the script categorizes each element into a layer and then appends the element list to the input file. Since the categorizing of the elements is not dependent on previous steps, the script was coded to execute in parallel. This was accomplished by splitting the elements into partitions, and then categorizing each partition of elements on an independent thread. Finally, the categorized elements from each thread is merged into a master list to be written to the output file.  In the input deck, the *STEP card was used in with the *MODEL CHANGE card to perform the addition of the layers, in CalculiX. Thus, the input deck is read once, while the laser information and material data (discussed in the next section) are read at every iteration. Figure 3.1 shows the overall flowchart of the implementation.

Figure 3.1 - Implementation flowchart, adapted from [26]

At a given time step, each layer of elements contains sintered and powdered material. The distinction is made by the material properties of the integration point. A layer is initialized with powered material properties. During runtime sintered material properties are assigned once the laser has passed over the integration point. This is the hybrid method as discussed in section 2.2 - AM Finite Element Simulation on page 11.

The mechanical simulation uses incremental pointwise plasticity as the material constitutive law, assuming isotropic hardening. Here, creep effects were neglected. This was implemented within a user material subroutine by a call to the incremental plasticity subroutine native to CalculiX. The plastic material properties used along with the rest of the material properties are discussed in the next section.

### Porosity and Material Properties

Internal, solution-dependent state variables are used to track the physical state of the material microstructure. Solution-dependent state variables in CalculiX exist for each integration point in the model. Thus, a single element can have different material properties at each of the integration points in a simulation. One solution-dependent state variable is used to store the current predicted porosity of the material and another to differentiate powder from sintered material. For visualization purposes, a third was used to store the current structural elastic modulus of the material.

CalculiX sources were modified to allow for a thermal and structural user material capable of altering material properties as determined by interpolating the material properties in a lookup table.  A predetermined table of material properties (discussed in the next section) were tabulated the material constitutive relationship (elastic modulus, Poisson's ratio, and plastic strain/stress pairs), thermal conductivity, specific heat, and thermal expansion coefficients as a function of temperature, material state (powder or solid) and volume fraction of air to solid (porosity) of the sintered material. How this precomputed table was populated is discussed shortly. This was accomplished by modifying the “materialdata_me.f” and “materialdata_th.f” subroutines in CalculiX to accept material properties from a third Fortran subroutine. This subroutine read the properties from the tabulated file and perform a 2D interpolation of the table (once for temperature and again for porosity). If the temperature or porosity being requested is out of bounds from the values specified in the table, the closest temperature or porosity in the table is used (no extrapolations).

The evolution of the porosity of the sintered material ε is predicted during runtime from Eq.  obtained from Ref. [14], where ε0 is the initial porosity of the powder (assumed here to be 0.3), and εmin is the minimum attainable porosity (assumed here to be 0.0001). The assumptions for the initial and minimum values of porosity are preliminary, used to establish the method. In the future, these properties will be measured. Note that, the densification coefficient K is a function of powder diameter, distribution, and material properties. Here, it was assumed to be constant at 18.97 mm3kJ, as a preliminary value from Ref. [14].

The specific energy input ψ is calculated using the laser power Pz, laser linear velocity v, and the laser beam area, characterized by l and w, as shown in Eq.  . Here, the product lw is taken as πr02. The volume fraction Vf of the sintered material is taken as Vf=1-ε that is Vf=1 represents 100% solid and Vf=0 represents 100% air. The laser penetration was assumed to exponentially decay into the material as shown in Eq.  [29], Kz is as defined in Eq. . It was also assumed that, the estimated porosity ε for an already sintered layer (the layers below the topmost layer) can be used as the initial porosity ε0 in Eq.  for subsequent passes of the laser, at each time step. Thus, the porosity of all the layers in the model change during the simulation.

Figure 3.2 shows a simplified illustration of the evolving porosity as the laser passes over the powder for the SLS process. Note that Eq.  is the empirical approximation to the solution to the underling differential equation , where κ (kappa) is the sintering rate constant. The sintering rate constant is a function of the laser specific energy input ψ. Note that Eq.  predicts the final porosity after a laser pass (no dependence on time), while Eq.  is time dependent. Both equations have been shown to be a reasonable representation to model to the real porosity evolution [14].

Figure 3.2 - Changing porosity

ε=-κε

The macroscopic homogenized material properties were precomputed using NASA’s Micromechanical Analysis Code – Generalized Method of Cells (MAC-GMC). A triply periodic open-cell RUC was chosen for the representative arrangement of the partially sintered material, as shown in Figure 3.3. In the figure, a dark blue rectangular subcell represents a solid material, and a translucent blue represents air. Note that this RUC is assumed to be isotropic, thus no need to store any anisotropic material properties.

GMC calculates the material properties in an average sense [24]. That is, the stress carried by the RUC in a direction is evenly carried across the subcells. Stress concentrations due to corners are not resolved. Thus, a spherical microstructure would effectively be represented as a rectangular cuboid subcell in GMC.

| - Vf= 66% | - Vf= 95% |
| --- | --- |

Figure 3.3 - Triply periodic open-cell RUC

Properties of solid Inconel 625 were used for the solid material, tabulated in Table 3-1. The mechanical properties of air (voids due to porosity) were estimated as 7 orders of magnitude smaller than the mechanical properties of the solid material. The computed sintered material properties are plotted in Figure 3.4 with respect to temperature. The figure shows that the yield strength and the stress for a given plastic strain decrease as the volume fraction decreases. A similar decrease in those properties can be seen as the temperature increases. All the material properties computed by MAC-GMC are tabulated in Table 8-1 in the appendix.

Table 3-1 - Solid Inconel 625 properties used as a function of temperature

| Temperature °C | 20 | 200 | 400 | 700 | 900 |
| --- | --- | --- | --- | --- | --- |
| E GPa | 204 | 193 | 181 | 161 | 145 |
| υ | 0.312 | 0.303 | 0.301 | 0.309 | 0.284 |
| ρ kgm3 | 2700 | 2700 | 2700 | 2700 | 2700 |
| k WmoC | 9.8 | 12.5 | 15.3 | 19.8 | 23.3 |
| C JkgoC | 410 | 456 | 511 | 600 | 630 |
| α 1°C | 12.6E-06 | 13.1E-6 | 13.6E-6 | 15.0E-6 | 1.60E-05 |
| Sy MPa | 618 | 610 | 491 | 501 | 195 |
| εp,1 | 0.036 | 0.0782 | 0.0670 | 0.1024 | 0.0535 |
| S1 MPa | 727 | 736 | 574 | 689 | 190 |
| εp,2 | 0.092 | 0.2469 | 0.1139 | 0.1584 | 0.2225 |
| S2 MPa | 803 | 876 | 625 | 721 | 167 |
| εp,3 | 0.204 | 0.3030 | 0.2387 | 0.4685 | 0.4908 |
| S3 MPa | 902 | 901 | 707 | 601 | 50 |

Figure 3.4 - Sintered material homogenized macroscopic stress-strain curve.

The powdered material properties were set equal to the sintered material properties, except for the modulus of elasticity, at a given temperature and volume fraction. The modulus was estimated to be an order of magnitude smaller than that of the sintered material for a given volume fraction at room temperature. As the temperature of the powder increases, the modulus of the powder was set to linearly increase, until 700 °C, at which the modulus of the powder was made the same to that of the sintered material, at a given volume fraction. This was done to avoid strong C1 discontinuities in material properties and to avoid the strain-softening of the solid Inconel at high strains and temperatures, aiding in numerical convergence. It was assumed that this slow change in powder material properties to sintered material modulus would not adversely affect the results since the spatial gradient of temperature is extremely high near the laser. Thus, the temperature of the powder material is close to room temperature a small distance away from the laser, and at room temperature, the powder material has a low modulus. These powder material estimates are preliminary and used to establish the methodology. In the future, these properties can be measured and the sensitivity of the results to these properties investigated. Figure 3.5 shows how this modulus changes with temperature and volume fraction. The solid line represents the linear interpolation used during runtime for temperatures not tabulated.

| - Elastic modulus vs. temperature at Vf=95% | - Elastic modulus vs. temperature vs. volume fraction |
| --- | --- |

Figure 3.5 - Elastic modulus vs. temperature vs. volume fraction.

## Results

### Boundary Conditions

The geometry used, along with the bed and mesh is shown in Figure 3.6. It is customary in literature that the cartesian coordinate system is oriented such that the positive z-direction is the build direction.  The dimensions of the printed part are 12 mm by 12 mm by 3 mm, while the bed is 9 mm by 1.5 mm by 18 mm. The mesh used linear 8-noded hexahedral elements. The bottom of the bed was set to a constant temperature of 70 °C, with no displacements. The elements in the mesh were approximately 1mm on each side. This allowed the heat flux from the laser beam (with a characteristic radius of 2.5 mm) to be applied to several integration points during a time step. The layer thickness was taken as 1mm; thus, one element was used through the thickness of a layer.

To avoid the computational cost of modeling the conductive heat flux into a physical region of excess powder, the heat carried away by the powder surrounding the part was modeled as an effective convective heat transfer boundary condition, to avoid the computational cost of modeling the conductive heat flux into a physical region of excess powder. Here it was assumed that the unmodeled powder changed temperature from its maximum at the surface of the part to its steady-state, far-field temperature within 10 mm. This gives an effective convective heat transfer coefficient of heff,powder=kL=362 Wm2K, with an estimated conductive coefficient of kpowder=3.62 WmK. The powder thermal conductive coefficient kpowderwas estimated from MAC-GMC with a volume fraction of 66%. A changing convective boundary condition was applied to the current topmost surface with a convection coefficient of hair=100 Wm2K. A radiation boundary condition was also applied to the current topmost surface. The effective absorption for the radiation was assumed to be 50%. The ambient temperature of the air was assumed to be 70 °C, as well as the bed preheat temperature. The bed preheat temperature was also set to 70 °C. Figure 3.7 illustrates these boundary conditions.

Bed

Part

A

B

Figure 3.6 - Geometry and mesh used.

Effective conduction to powder

Fixed displacements and fixed temperature at 70°C

Radiation to environment at 70°C, 50% emissivity, Convection to environment at 70°C

Figure 3.7 - Boundary conditions applied.

Figure 3.8 shows the scanning pattern used. The laser path was discretized into time steps of 0.05 seconds for the FE simulation, as shown. The same path was used for all the layers. At a laser speed of 100 mm/s (as shown in Table 3-2), a layer was scanned in about 5 seconds. With a dwell time (time between layers) of 1 second per layer, and 12 layers in the model the total simulated print time is 72 seconds. A dwell time of a second was enough to cool the part to ambient temperature in the simulation. Values used for the laser properties for Eq.  are listed in Table 3-2, adapted from Ref. [21].

Table 3-2 - Laser parameters

| η | r0 mm | s mm | P W | v mms |
| --- | --- | --- | --- | --- |
| 1 | 2.5 | 1 | 2,250 | 100 |

Starting point

Overall scan direction

Figure 3.8 - Laser beam scanning path.

### Evolving Porosity

Post-processing was accomplished with the open-source software ParaView. Figure 3.9 shows the results of the simulation at the midpoint of part completion. Figure 3.10 shows the results at the end process after cooling. Corresponding graphs are shown at the same scale.

| - Modulus, MPa | - Sxx, MPa |
| --- | --- |
| - Temperature, °C | - Syy, MPa |
| - Porosity | - Szz, MPa |

Figure 3.9 - Results at t = 31.5s, evolving porosity, no deformation shown.

| - Modulus, MPa | - Sxx, MPa |
| --- | --- |
| - Temperature, °C | - Syy, MPa |
| - Porosity at end of print | - Szz, MPa |

Figure 3.10 - Results at the end of print, t = 72s, deformation magnified by 20x, evolving porosity.

Figure 3.11 shows the estimated porosity evolution at a specific node in the model. It shows that the predicted porosity decays from its initial value to its minimum value in approximately a second. The abrupt change in slope in the porosity vs. time plot corresponds with the position of the laser relative to the point in the material.

C

Figure 3.11 - Estimated porosity vs. time, at node point C.

The stresses in Figure 3.9 and Figure 3.10 on page 49, subplots b, d, and f show that there are primarily compressive residual stresses on the outer surfaces while tensile towards the center. In addition, there are stress concentrations where the part meets the bed, as expected. In addition, the residual stresses in the z-direction are the greatest compared to the other two orthogonal stresses.

The porosity plot in Figure 3.10 subplot e shows that there is still some porosity at the top surface. This could be due to the laser having passed over the top surface only once. The temperature plot in Figure 3.9 subplot c, shows that the temperature is greater inside the part than at the top surface. This temperature gradient may be explained by the convective and radiative boundary conditions on the surface combined with the volumetric heat flux. The temperature dependence of the elastic modulus can also be seen in Figure 3.9 subplot a.

The deformation in Figure 3.10, shows that the part swells at the center, with a small amount of deformation towards the top horizontal edges. This behavior also is seen during the simulation of the process, not just after part completion. In addition, the top four corners of the part tend to point in the positive z-direction.

### Constant Porosity

A second model with a constant porosity of 10% was simulated for comparison. All other parameters including the mesh were kept the same as the previous evolving porosity simulation. Corresponding graphs are shown at the same scale as the previous simulation. The material properties were taken as only dependent on temperature and material state (powder or sintered). Figure 3.12 and Figure 3.13 shows the results of this simulation.

| - Modulus E, MPa | - Sxx, MPa |
| --- | --- |
| - Temperature, °C | - Syy, MPa |
|  | - Szz, MPa |

Figure 3.12 - Results at t = 31.5s, constant porosity, no deformation shown.

| - Modulus, MPa | - Sxx, MPa |
| --- | --- |
| - Temperature, °C | - Syy, MPa |
|  | - Szz, MPa |

Figure 3.13 - Results at the end of print, t = 72s, deformation magnified by 20x, constant porosity.

The elastic modulus plot in Figure 3.12 subplot a shows that compared to Figure 3.10 subplot a, the change in the material's modulus from sintered to powder is more severe. This can adversely impact numerical convergence.

Figure 3.12 and  Figure 3.13 show a similar trend in residual stresses at the end of the printing simulation and similar temperatures during the printing of the part. However, comparing subplots f (stresses in the z-direction), the evolving material model tends to show greater stresses in magnitude.

Table 3-3 shows a comparison of residual stresses and distortions, at surface points A and B labeled on the geometry used in Figure 3.6. The table shows that the differences in the models can be significant and that the evolving porosity model does not always give greater residual stresses or distortions.

Table 3-3 - Residual stress and distortion comparison.

|  | Point A |  |  | Point B |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Constant Porosity | Evolving Porosity | % increase in magnitude | Constant Porosity | Evolving Porosity | % increase in magnitude |
| Sxx MPa | -77 | -55 | -29% | -450 | -364 | -19% |
| Syy MPa | -60 | -16 | -73% | -11 | -1 | -91% |
| Szz MPa | -210 | -246 | 17% | -38 | -47 | 24% |
| Uxx mm | -.00894 | -.016807 | 88% | .001025 | .000541 | -47% |
| Uyy mm | .000809 | .006235 | 671% | .000174 | -8.42e-5 | -148% |
| Uzz mm | -.002287 | -.013365 | 484% | .002095 | .001269 | -39% |

## Discussion and Conclusion

Figure 3.14 shows a comparison of the von Mises stress at the final print time, after cooldown. The figure shows that that modeling an evolving porosity results in higher overall residual stresses with larger deformations. The models show a similar stress distribution trend, with evolving model having slightly higher magnitudes. These observations can also be seen comparing subplots b, d, and f of Figure 3.10 and Figure 3.13. The equivalent plastic strain in the models is compared in Figure 3.15; again, it shows a similar distribution, with higher magnitudes. Both models used the same laser parameters, boundary conditions, and mesh.

| - Evolving porosity model | - Constant porosity model |
| --- | --- |

Figure 3.14 - Von Mises stress, at t=72s, deformation magnified by 20x

| - Evolving porosity model | - Constant porosity model |
| --- | --- |

Figure 3.15 - Equivalent plastic strain, at t=72s, deformation magnified by 20x.

The peak positive normal stress in the z-direction was calculated at 230 MPa for the evolving porosity model, while the constant porosity model showed a peak positive stress of 145 MPa. The evolving model had a peak displacement of 0.027 mm while the constant model had a peak displacement of 0.016 mm.

This increase in deformation and residual stresses is likely due to the regions with high porosity having to carry the same load (due to thermal strains and constraints by the surrounding material) yet with a lower microscopic cross-sectional area. This reduced cross-sectional area can be seen by comparing the microscopic architectures in Figure 3.3. The higher applied stresses may result in higher plastic strains, leading to higher residual stresses at part completion and higher part deformation.

These results show that including microscale phenomena, specifically the porosity, may lead significant changes in the predicted macroscopic fields. Although including microscale phenomena adds more complexity (and slightly more computational time), this addition may lead to more accurate results. Thus, it may be important to model this and other microscale phenomena, such as grain orientation. This work lays the foundation for including anisotropic thermal and mechanical material properties as well as the addition of material microstructure evolution and other microstructural effects.

A limitation of this work is that to date, no experimental validation has been conducted on the presented work. This includes validation on the porosity model used in addition to the predictions made by the simulation. Furthermore, it is expected that the mesh used here is not able to resolve the fine details in the solution.

This work used the densification coefficientcoupled to a time-dependent thermal history, to yield an evolving volume fraction. The volume fraction is used with GMC to provide predictions of temperature and volume fraction dependent stress-strain and plasticity at the micro-scale. These material properties, used in a macro-scale finite element model, compute evolving volume fraction dependent residual stresses.  In short, evolving volume fractions impact porosity and consequently impact the residual stresses and deformation.

CHAPTER 4

# Effects of Geometry with Inherent Strain

Due to the limitations of the full thermomechanical method, the inherent strain method was used here to obtain results in a practicable time frame, at the cost of some approximations in the solution. Despite these approximations (as described in section 2.2.2 - The Inherent Strain Method on page 20) the advantage of fast computational times may outweigh the disadvantages, making it possible to obtain the final residual stresses and distortions of  relatively large structures. For simple models (such as the cantilever beam with supports) the inherent strain method has shown to produce satisfactory predictions comparing to experimental results [12]. Here the inherent strain method along with a dense mesh is used to study the effects of geometry on the overall distortion and stress on the parts, despite Ref. [3] suggesting that the ISM can lead to inaccurate results when applied to various geometries. Some of these geometries are then compared against the full thermomechanical method not only for accuracy but for similar trends. Again, it is not the goal of this chapter to produce accurate results validated experimentally, but to show trends.

## Methodology and Implementation

The inherent strain applied was chosen as the volume averaged plastic strain as computed with the thermomechanical model used in Chapter 3 - Effects of an Evolving Porosity. In addition, since each element layer represents many AM layers, it was assumed that the inherent strain was the same in the build plane (the x-y plane), since during manufacturing, the laser scan pattern is rotated  at every layer to avoid the accumulation of stress [12]. Furthermore, since each AM layer is thin in the build-direction (the z-direction), it was assumed that the inherent strain in this direction was zero. Thus, the applied inherent strain for these models is: ε*=εxxεyyεzzεxyεxzεyzT=-.004-.0040000T. These values are approximately the same values as calibrated numerically and from experiments in Ref. [3]. Note that these strains are a strong function of processing parameters [3].

To implement this method with CalculiX, a few minor modifications to its source code were needed. This modification allowed the inherent strains to be applied at a set of elements. Unmodified, CalculiX only allows the specification of one initial strain at one integration point in one element at a time, impracticable for this application. Two steps in CalculiX were required to simulate and load the layer. This is because adding a set of elements (a layer) requires artificially adding strains to the newly added layer, since the layer before is already strained, thus the new elements are deformed, yet with no stress. A second step then loads the whole layer at a time with the inherent strain. Section 2.2.2 - The Inherent Strain Method on page 20 reviews the method.

## Geometry and Validation

A cube 10 mm to a side with a blind hole 5 mm deep was chosen as the geometry due to its simplicity. The diameter of the hole was varied from 0 mm (no hole) to 8 mm, producing nine specimens. Quadratic 20-noded brick elements with a global size of 0.5 mm on a side were used. Figure 4.1 shows the mesh used for the geometry with a 6 mm diameter hole. The bottom nodes were constrained with no displacements (surface denoted by dashed lines in the figure). The inherent strain was applied at every layer, each layer being 0.5 mm thick (one quadratic element thick).

Figure 4.1 - Geometry of 10 mm cube, Ø 5 mm, 5 mm blind hole

For stress distribution validation predicted by the inherent strain model, a coarsely meshed thermomechanical model was simulated. Material properties of Inconel 625 at room temperature and fully dense were used for the inherent strain model. The geometry and boundary conditions in Figure 4.1 were used for the inherent strain model. Similar boundary conditions and laser scan pattern as in Chapter 3 were used for the thermomechanical model.

Figure 4.2 shows the von Mises stress at the mid-cross-section of the part. Note that all three plots have the same deformation magnification, but the right plot (thermomechanical simulation) has a different scale on stress. The figure shows similar (although not exact) deformations between the two methods, with similar overall trends in stress distribution. A major difference in deformation being the thin walls surrounding the hole. The inherent strain method predicts wrapping here while the thermomechanical method does not. The thermomechanical method used also predicts smaller stress magnitudes. In addition, the inherent strain method shows smoother contours of stress compared to the thermomechanical model. This, however, is likely explained by the course mesh used for the thermomechanical model. The inherent strain method also produced overall tensile stress at the outer surfaces, while compressive stresses towards the center of the part, as expected from a literature review. Despite these differences, the distribution of stress and displacement are similar between the two models. Thus, it is assumed that the inherent strain model is capable of producing accurate trends in stress distribution and deformation with respect to the geometry.

| Inherent strain |  | Thermomechancial |
| --- | --- | --- |
| Coarse mesh ≅1 mm | Fine mesh ≅0.5 mm | Coarse mesh ≅1 mm |

Figure 4.2 - Inherent Strain and thermomechanical comparison, 8 mm diameter, deformation magnified 20x

Figure 4.3 - Cantilever beam deformation, before (top) and after (bottom) stress release, no deformation magnification

This inherent strain was then applied to a finely meshed (≅ 0.5 mm cube linear hexahedral elements) supported cantilever 100 mm long, 3 mm thick, 10 mm wide beam model. Material properties of room temperature Inconel 625 used. Supports are 10 mm long (in the z-direction). Stress and deformation are shown in Figure 4.3. The tip displacement is at 4.7 mm. Buchbinder et al. in Ref.  [30] obtain tip displacements in the range 1 – 8 mm for a 50 mm long and 0.5 – 5 mm thick beam specimens made from ALSi10Mg aluminum alloy. Different tip displacements were obtained due to different preheat temperatures.  Liang et al. in [22] obtained a displacement of 0.58 mm with 76.6 mm long beam made from Inconel 718. Clearly the tip displacement is highly dependent on processing parameters (and obviously material), thus such a comparison may not be adequate. However, the overall shape, order of magnitude of deformation, and stress distribution agrees with the literature [31]. A calibration with experimental testing is needed to obtain more accurate results.

## Results

The hole diameter of the nine specimens are show in Table 4-1 along with the volume averaged von Mises stress (i.e. Savg,vm=1VSvmdV). Volume averaged quantities were chosen for comparison since each specimen has different volumes. Plots showing the von Mises stress distribution is shown in Figure 4.4. All plots shown at the same scale.

Table 4-1 - Inherent strain, geometrical feature  results

| Hole diameter (mm) | Volume (mm3) | Max displacement (mm) | Max von Mises (MPa) | Volume averaged von Mises (MPa) |
| --- | --- | --- | --- | --- |
| 0 (no hole) | 1000 | 0.081734 | 768.83 | 452.59 |
| 1 | 996.14 | 0.081363 | 773.39 | 454.05 |
| 2 | 984.35 | 0.08041 | 783.29 | 455.51 |
| 3 | 964.78 | 0.078917 | 793.19 | 456.21 |
| 4 | 937.27 | 0.076971 | 800.11 | 451.98 |
| 5 | 901.98 | 0.074356 | 801.15 | 443.58 |
| 6 | 858.83 | 0.071471 | 798.48 | 436.18 |
| 7 | 807.70 | 0.068305 | 797.39 | 430.85 |
| 8 | 748.8 | 0.065311 | 799.81 | 429.65 |

| - 0 mm diameter | - 1 mm diameter | - 2 mm diameter |
| --- | --- | --- |
| - 3 mm diameter | - 4 mm diameter | - 5 mm diameter |
| - 6 mm diameter | - 7 mm diameter | - 8 mm diameter |

Figure 4.4 - Von Mises stress of geometry with various hole diameter, deformation magnified 20x

Figure 4.5 - Hole diameter effects, inherent strain

The plots in Figure 4.4 show that the hole acts to reduce the stress near the bottom surface of the hole. This is presumably due to the traction free surface at the bottom of the hole. Figure 4.5 shows how the output results (volume averaged von Mises stress, maximum von Mises stress, and maximum displacement) vary as a function of the diameter. Note that the vertical axes do not start at zero. As shown in plots a and b, of Figure 4.4, the stress distribution around the small diameter hole is relatively unaffected by the presence of the hole. This may explain the initial increase in the averaged stress in Figure 4.5, as the average stress would increase due to the absence of material (s mall stress not present due to the absent material that would otherwise decrease the average). The maximum stress observed occurred at the bottom where the clamped boundary condition was applied, as expected.

The maximum displacement occurred at the four outer vertical edges of the cube for all the specimens. It may be reasoned that the maximum displacement decreases as the diameter increases due to the negative inherent strain applied in equal magnitudes in the x and y direction at a whole layer, thus contracting the circular walls inward. This is different from the thermomechanical model where the load is applied only where the laser is currently located.

## Discussion and Conclusion

The results shown in Figure 4.5 that the diameter of the blind hole has an effect on the volume averaged von Mises stress as well as the maximum displacement and stress. Note that maximum stress can be dependent on stress concentrations which are in turn dependent on geometry. However, the corner radii of all the corresponding corners in the model are kept constant, at an ideal 90 degrees. It is also important to note that these results may be skewed due to boundary effects, as the hole approaches the edge of the specimen with larger diameters. These results support the hypothesis that the macroscale geometry influences the residual fields.

CHAPTER 5

# Geometry Effects with Thermomechanical FEA

To further asses the effects of geometry on the solution, a slightly more complex geometry was investigated using the thermomechanical model developed in Chapter 3. Investigating more geometrical variables may prove beneficial to evaluate the geometry effects. Using the thermomechanical model would also make possible to circumvent some of the disadvantages of the inherent strain method (discussed in section 2.2.2 - The Inherent Strain Method). This required a few modifications to the implementation used in Chapter 3, since significant numerical convergence problems were encountered when applying the developed model to larger geometries.

## Methodology and Implementation

Modifications to the thermomechanical model include incorporating a viscoplasticity material constitutive model. Viscoplasticity aids in numerical convergence by allowing the stress state to exceed the yield surface, this being a less restrictive constraint for the solver. This is possible since the material response is time dependent, thus the response (stress) of the material is higher at higher strain rates. In contrast, incremental plasticity requires the stress state to lay on the yield surface when yielding (steady state). Implementing this material model in CalculiX with the user subroutines described in Chapter 3 simply required calling the built-in viscoplasticity model. The viscoplasticity model used is the power creep law as shown in Eq. , where A,n,m are temperature dependent material properties, σ is von Mises stress and ε is the steady state strain rate, such that the total strain is εtotal=εelastic+εinelastic+εt.

A limitation with the implementation is that constant viscoplasticity material properties where used. Typically, the viscous properties of materials are highly temperature dependent. However, it may be reasoned that since the temperature quickly increases (within milliseconds in the models) from room temperature to melting temperature and back to room temperature (with in approximately a second in the simulations), and because strains near melting temperatures have less impact on stress than those at lower temperatures, viscoplasticity properties at high temperature may not be as important as those at lower temperatures.

Another modification to the implementation described in Chapter 3 includes using the porosity model shown in Eq.  (repeated below in Eq.  for reading convenience). Note that ε in Eq.  refers to porosity rate opposed to strain rate in Eq. . The differential was solved numerically in the DFLUX subroutine in CalculiX using forward Euler, since κ is a function of the laser specific power. Regression coefficients from Ref. [14] where used.

ε=-κε

A final modification included the ability to apply a different laser pattern at every layer. This is necessary if the cross-sectional geometry changes at every layer. This was accomplished by storing laser position in a 3D table for look-up at runtime.

Linear 8-nodded hexahedral elements were used with approximately 1 mm in the x-direction and y-direction dimensions while 0.5 mm was used in the z-direction. This was done to add two layers of elements at every additional AM simulated layer, while keeping the thickness of the AM layer at 1 mm. This is different from what was done in Chapter 3, where only one layer of elements was added at a time. Preliminary mesh convergence studies (not presented in this document) showed that adding two layers of elements at a time provided more refined results that were similar to literature [32].

As a preliminary validation, a cantilevered beam geometry was simulated. Figure 5.1. shows the deformation and stress of the specimen before (translucent) and after removing it from its base (relieving some stress). The deformation shown is consistent with the literature. The tip displacement for this 100 mm long and 3 mm thick beam is 0.52 mm. Again comparing to Liang et al. in reference [22], 0.58 mm was measured expermentally from a 76.6 mm long beam (thickness dimension not given). Note that this displacement is also highly dependant on processing parameters (laser scan pattern, preheat tempreture ect.). Thus, this comparison might not be adequate, but it shows that the simulaiton has a reasonable solution.

Figure 5.1 - Preliminary cantilevered beam simulation

## Results

A nozzle-shaped geometry with three geometric parameters to be varied was chosen, shown in Figure 5.2. This geometry is simple enough to model with few parameters yet complicated enough to produce interesting results.

Figure 5.2 - Geometry and varied parameters

To obtain a distribution of this sample space and to avoid a large amount of simulations, Latin hypercube sampling (LHS) was used. Latin hypercube sampling has the advantage that it can lead to a faster converged results with fewer sample points compared to the Monte Carlo method [33]. This is done by dividing the normal cumulative function into n ranges and sampling each range, where n is the number of desired trials/experiments. Then for a given variable, it is assigned one of the n ranges for every trial, unique at every trial. The value of that variable is then obtained from the inverse cumulative function using the value from its assigned range. This assignment of a range to a variable can be random or it can be optimized to maximize the Euclidean distance between each of the trials in the sample space. This was done here using libraries in the R programing environment.

Figure 5.3 - Sampled LHS inputs

Here, 30 sample points were chosen; specimens whose solution converged (24 of the 30) are shown in Figure 5.3 and Table 5-1. A representative mesh used along with its laser 3D scan pattern is shown in Figure 5.4. The laser pattern is rotated by 90 degrees at every layer. Similar boundary conditions to that of Chapter 3 were used.

Figure 5.4 - Representative mesh and laser scan pattern, specimen #1

Table 5-1 - Sampled LHS inputs

| Specimen | Thickness (mm) | Radius (mm) | Length (mm) |
| --- | --- | --- | --- |
| 1 | 4.632 | 9.012 | 16 |
| 3 | 2.209 | 8.372 | 14 |
| 6 | 3.180 | 8.308 | 20 |
| 7 | 4.568 | 7.736 | 8 |
| 8 | 3.938 | 10.902 | 18 |
| 9 | 3.354 | 11.310 | 8 |
| 11 | 2.022 | 9.904 | 10 |
| 12 | 3.725 | 8.723 | 12 |
| 13 | 4.928 | 10.077 | 12 |
| 14 | 3.529 | 9.377 | 6 |
| 16 | 4.817 | 10.170 | 20 |
| 17 | 3.462 | 8.878 | 16 |
| 18 | 2.707 | 7.910 | 10 |
| 19 | 3.090 | 10.480 | 10 |
| 20 | 2.542 | 9.298 | 8 |
| 21 | 3.664 | 9.803 | 16 |
| 22 | 2.325 | 7.552 | 18 |
| 23 | 2.136 | 9.513 | 12 |
| 24 | 4.776 | 8.127 | 14 |
| 25 | 4.139 | 11.961 | 8 |
| 26 | 4.407 | 11.659 | 6 |
| 27 | 3.281 | 10.731 | 14 |
| 28 | 3.857 | 11.129 | 18 |
| 30 | 2.942 | 8.516 | 10 |

Figure 5.5 shows a representative von Mises stress plot (same specimen shown in Figure 5.4) before and after the clamped boundary conditions at the bottom are removed. Removing of these boundary conditions simulated the part being cut off from the building bed. The intended undeformed geometry is also shown in the background for reference. Similarly, Figure 5.6 shows the same plot at the mid cross-section. Parallel camera projection was used for these figures for comparison with original geometry.

Figure 5.5 - Representative von Mises stress plots, before (left) and after (right) stress relieving, deformation magnified by 100x, specimen #1

Figure 5.6 - Representative von Mises stress plots, before (left) and after (right) stress relieving, deformation magnified by 100x, specimen #1

Figure 5.7 - Representative stress plots, before (left) and after (right) stress relieving, deformation magnified by 100x, specimen #1

As shown in the previous figures, the deformation of the part significantly increases while its stress decreases after the part is removed from its clamped conditions, as expected. The figures also show that this deformation after removing is greatest near the bottom. This is likely due to the clamped condition giving rise to higher plastic strain since the material is being constrained. Figure 5.5 that there are point-like areas of higher von Mises stress throughout the part, especially towards the top. This is likely due to the scanning pattern used. Figure 5.7 shows that as expected the solution produced tensile stresses towards the outer surfaces (especially at the inner surface) while compressive towards the center.

Figure 5.8 shows 3D scatter plots of the results obtained for all the specimens, before removing the clamped boundary conditions. The radius and thickness are shown in the x and y axes, while the length is shown by color and by the size of the points in the plots. The variable chosen of interests are the maximum von Mises stress, maximum diametrical displacement (change of the nozzle diameter), the volume averaged magnitude of displacement, and the volume averaged von Mises stress. The maximum von Mises plot (upper left) shows a correlation between this and the radius of the part. Likewise, a correlation can be seen between the volume averaged displacement and the radius of the part (lower left). Other correlations are difficult to visually observe.

Figure 5.8 - Solution at the end of print, before removing from bed

Figure 5.9 shows the results after removing the clamped boundary conditions. In addition to the two correlations observed previously (max stress and average displacement), the figure shows a positive linear correlation with the maximum diametrical displacement (upper right plot) and radius.  This maximum displacement (shrinkage of the diameter) occurs at the base of the part where the clamped boundary condition is applied. This correlation is expected, as a larger initial distance (diameter in this case) will produce a larger end displacement (diameter change), assuming a constant strain.

Figure 5.9 - Solution at the end of print, after removing from bed

A linear and quadratic regression was performed on the results to quantify the above observations, using the R programming environment. Partial results of the linear regression are shown in Table 5-2, with the full table and quadratic regression results in the appendix. p-values less than 5% are accepted as indicating a statistically significant correlation coefficient whereas the coefficients themselves indicate the magnitude of the impact of the independent variable. The observations described from the plots are corroborated by the coefficients and p-values.

Table 5-2 - Linear regression results; partial table; MPa - mm units

| Linear Regression |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Dependent Variable | Independent Variable | Before Stress Relief |  | After Stress Relief |  |
|  |  | Coefficient | Pr(>¦t¦) | Coefficient | Pr(>¦t¦) |
| Max Svm | (Intercept) | 1228.1 | 2.03E-09 | 1003.286 | 1.07E-05 |
|  | Thickness | -44.3 | 0.009931 | -22.178 | 0.33455 |
|  | Radius | -49.8 | 0.000208 | -48.936 | 0.00586 |
|  | Length | 1.29 | 0.702959 | 4.767 | 0.33582 |
|  | R-squared | 63.28% |  | 45.99% |  |
|  | P-value | 3.44E-05 |  | 0.005572 |  |
| Max. Udia | (Intercept) | 0.007143 | 4.55E-01 | 0.0051935 | 4.68E-01 |
|  | Thickness | -0.000135 | 0.913 | -0.000869 | 0.3527 |
|  | Radius | 0.0003842 | 0.661 | 0.0035903 | 0.0000197 |
|  | Length | 0.0001082 | 0.685 | -0.000372 | 0.0732 |
|  | R-squared | 1.42% |  | 68.97% |  |
|  | P-value | 0.9613 |  | 2.59E-05 |  |
| Avg. Svm | (Intercept) | 259.18 | 8.17E-05 | 137.193 | 2.09E-03 |
|  | Thickness | 0.7344 | 0.915679 | -3.619 | 0.48237 |
|  | Radius | -3.4792 | 0.481122 | -1.723 | 0.63521 |
|  | Length | -7.0895 | 0.000108 | -1.746 | 0.12477 |
|  | R-squared | 54.30% |  | 0.153 |  |
|  | P-value | 0.001122 |  | 0.3338 |  |
| Avg. Umag | (Intercept) | -0.000802 | 8.31E-01 | 0.002199 | 5.43E-01 |
|  | Thickness | -0.000373 | 0.4496 | -0.000427 | 0.3657 |
|  | Radius | 0.000672 | 0.0636 | 0.002071 | 0.00000348 |
|  | Length | 0.0000556 | 0.5993 | -0.000328 | 0.0036 |
|  | R-squared | 16.27% |  | 77.36% |  |
|  | P-value | 0.3033 |  | 1.04E-06 |  |

Figure 5.10 - Quadratic regression fitted plots, before stress release

Figure 5.10 and Figure 5.11 show the fitted curves for a quadratic regression. Regression statistics are tabulated in the appendix (Table 8-4). Again, the size of the points corresponds to the length geometric parameter. As expected, a quadratic regression provides higher R2 values, as the regression can capture some curvature.

Figure 5.11 - Quadratic regression fitted plot, after stress release

## Discussion and Conclusion

All the R2 values in Table 5-2 are less than 80%, indicating that the regression is not perfect, hinting that there is noise in the simulation results. Even though each simulation is completely deterministic from its given inputs, it is possible that the approximations required by the thermomechanical FE simulations (coarse mesh, oversized laser diameter, oversized element layers etc.) in combination with the additional assumptions and approximations made in the implementation (laser pattern, boundary conditions, etc.) lead to spurious  noise in the results. These assumptions and approximations are discussed in section 2.2.1 - The Thermomechanical FE Method, in section 3.1 - Implementation, and in section 3.2.1- Boundary Conditions. In addition, it is possible that the simulation results are extremely sensitive to other simulation parameters not tested such as thermal boundary conditions, maximum temperature laser scan pattern, porosity model, etc.

Figure 5.10 shows the predicted porosity for a representative specimen. It shows that the part is not completely dense. It is likely this is not realistic. This is a drawback of using a coarse laser scanning pattern (shown in Figure 5.4 on page 71), required by the larger laser diameter compared to what is physically used in AM. The areas of high porosity in Figure 5.10 correspond to areas where the laser did not cover. This may be a source of some of the noise seen in the stress plots (Figure 5.5, Figure 5.6, and Figure 5.7).

Figure 5.12 - Representative porosity, no deformation shown, specimen #1

Nonetheless, the results indicate that there is a statistically significant dependence of   the three varied dimensions (length, thickness, and radius) on the four chosen output variables (maximum diametric displacement, maximum von Mises stress, average von Mises stress, and average displacement). The sensitivity of the simulation results on the three geometrical parameters are shown by the regression coefficients in Table 5-2. Thus, it may be possible to influence the residual displacements and residual stresses by varying the overall geometry.

CHAPTER 6

# Conclusion

Despite the tremendous advantages of metal additive manufacturing, the distortions and residual stresses produced require post-treatments to mitigate. Thus, reducing or minimizing these fields before or during the manufacturing process is highly desired, aiding to reduce the required post-treatments. This necessitates a computational simulation of the process to predict the residual fields. This work presents a multiscale thermomechanical simulation capable of capturing the microscale evolving porosity phenomena. The simulation showed that modeling the porosity can have a significant effect on the predicted residual stress and residual deformations. Thus, it may be important to include this and other microscale phenomena into thermomechanical simulations of metal additive manufacturing. Although inclusion of these microscale phenomena requires slightly more computational power and increases the simulation complexity and number of properties required, it has the potential to obtain more accurate results at a slight increase in computational requirements. It also lays the foundation to incorporate other microscale phenomenon such as anisotropy for the SLS process and melting, laser melt tracks, and layering effects for the SLM process as well.

In addition to the work presented here, CalculiX sources have been modified to perform a super-integration scheme in calculating the mass, stiffness, and force matrices/vectors. The thermomechanical simulation implemented here necessitates a laser diameter comparable to the size of the elements, or else the energy of the laser will not be captured. This is due to small number of integration points in Gaussian quadrature (2 points in every direction for a linear hexahedral element). Performing a super integration scheme would allow for smaller laser diameters to be used closer to physical reality. 5-point and 10-point integration schemes were implemented.

A study on how the geometry affects the predicted residual fields is also presented, using the implemented computer simulation. The linear correlation between the geometry and the residual fields show that the geometry can indeed have a predictable effect on the residual fields. This predictability is important to producing an optimized geometry in a larger study.

It is important to note that a major limitation of this thesis is the absence of experimental validation. It is possible (and even probable) that there exist several discrepancies between the results presented here and experimentally measured quantities, since these models have not been calibrated.  However, it is not the goal of this work to produce validated results, but to merely demonstrate trends and distributions. The conclusions described here should not change due to these discrepancies.

References

# References

[1]	W. Xing, D. Ouyang, N. Li, and L. Liu, “Estimation of residual stress in selective laser melting of a Zr-based amorphous alloy,” Materials (Basel)., vol. 11, no. 8, 2018.

[2]	P. Mercelis and J. P. Kruth, “Residual stresses in selective laser sintering and selective laser melting,” Rapid Prototyp. J., vol. 12, no. 5, pp. 254–265, 2006.

[3]	M. Bugatti and Q. Semeraro, “Limitations of the inherent strain method in simulating powder bed fusion processes,” Addit. Manuf., vol. 23, no. May, pp. 329–346, 2018.

[4]	C. Li, Z. Y. Liu, X. Y. Fang, and Y. B. Guo, “Residual Stress in Metal Additive Manufacturing,” Procedia CIRP, vol. 71, pp. 348–353, 2018.

[5]	L. Wang, X. Jiang, Y. Zhu, X. Zhu, J. Sun, and B. Yan, “An approach to predict the residual stress and distortion during the selective laser melting of AlSi10Mg parts,” Int. J. Adv. Manuf. Technol., vol. 97, no. 9–12, pp. 3535–3546, 2018.

[6]	K. Carpenter and A. Tabei, “On residual stress development, prevention, and compensation in metal additive manufacturing,” Materials (Basel)., vol. 13, no. 2, 2020.

[7]	K. Moussaoui, W. Rubio, M. Mousseigne, T. Sultan, and F. Rezai, “Effects of Selective Laser Melting additive manufacturing parameters of Inconel 718 on porosity, microstructure and mechanical properties,” Mater. Sci. Eng. A, vol. 735, no. August, pp. 182–190, 2018.

[8]	A. Kreitcberg, V. Brailovski, and S. Turenne, “Effect of heat treatment and hot isostatic pressing on the microstructure and mechanical properties of Inconel 625 alloy processed by laser powder bed fusion,” Mater. Sci. Eng. A, vol. 689, no. January, pp. 1–10, 2017.

[9]	M. Shiomi, K. Osakada, K. Nakamura, T. Yamashita, and F. Abe, “Residual stress within metallic model made by selective laser melting process,” CIRP Ann. - Manuf. Technol., vol. 53, no. 1, pp. 195–198, 2004.

[10]	F. Cao, T. Zhang, M. A. Ryder, and D. A. Lados, “A Review of the Fatigue Properties of Additively Manufactured Ti-6Al-4V,” Jom, vol. 70, no. 3, pp. 349–357, 2018.

[11]	P. J. Withers and H. K. D. H. Bhadeshia, “Residual stress part 1 - Measurement techniques,” Mater. Sci. Technol., vol. 17, no. 4, pp. 355–365, 2001.

[12]	I. Setien, M. Chiumenti, S. van der Veen, M. San Sebastian, F. Garciandía, and A. Echeverría, “Empirical methodology to determine inherent strains in additive manufacturing,” Comput. Math. with Appl., vol. 78, no. 7, pp. 2282–2295, 2019.

[13]	S. . Furrer, D.U. Semiatin, “ASM Handbook, Volume 22B - Metals Process Simulation - 16.2 Fundamentals of Process Modeling,” ASM Int., pp. 240–252, 2010.

[14]	Y. Yang, O. Ragnvaldsen, Y. Bai, M. Yi, and B. X. Xu, “3D non-isothermal phase-field simulation of microstructure evolution during selective laser sintering,” npj Comput. Mater., vol. 5, no. 1, 2019.

[15]	P. Peyre, P. Aubry, R. Fabbro, R. Neveu, and A. Longuet, “Analytical and numerical modelling of the direct metal deposition laser process,” J. Phys. D. Appl. Phys., vol. 41, no. 2, 2008.

[16]	M. Jamshidinia, F. Kong, and R. Kovacevic, “Numerical modeling of heat distribution in the electron beam melting® of Ti-6Al-4V,” J. Manuf. Sci. Eng. Trans. ASME, vol. 135, no. 6, pp. 1–14, 2013.

[17]	C. K. A. BaurereiB, T. Scharowsky, “Defect generation and propagation mechanism during additive.pdf,” J. Mater. Process. Technol., 2014.

[18]	D. S. M. Robert D. Cook, Concepts and Applications of Finite Elemetn Analysis. 2001.

[19]	F. Hajializadeh and A. Ince, “Short review on modeling approaches for metal additive manufacturing process,” Mater. Des. Process. Commun., vol. 2, no. 2, pp. 1–7, 2020.

[20]	P. Ostiguy et al., “Fast prediction of thermal distortion in metal powder bed fusion additive manufacturing.” 2018.

[21]	S. Jayanath and A. Achuthan, “A Computationally Efficient Finite Element Framework to Simulate Additive Manufacturing Processes,” J. Manuf. Sci. Eng. Trans. ASME, vol. 140, no. 4, pp. 1–13, 2018.

[22]	X. Liang, Q. Chen, L. Cheng, D. Hayduke, and A. C. To, “Modified inherent strain method for efficient prediction of residual deformation in direct metal laser sintered components,” Comput. Mech., vol. 64, no. 6, pp. 1719–1733, 2019.

[23]	K. Krabbenhøft, “Basic Computational Plasticity,” Technical University of Denmark, 2002. .

[24]	J. Aboudi, S. M. Arnold, and B. A. Bednarcyk, Materials, 1st ed. Elsevier, 2013.

[25]	G. Dhondt, “CalculiX CrunchiX USER ’ S MANUAL,” 2012.

[26]	L. F. Silva, F. A. Yapor Genao, E. J. Pineda, and P. A. Gustafson, “Evolving Material Porosity on an Additive Manufacturing Simulation with the Generalized Method of Cells,” no. January, pp. 1–14, 2020.

[27]	B. Cheng, S. Shrestha, and K. Chou, “Stress and deformation evaluations of scanning strategy effect in selective laser melting,” Addit. Manuf., vol. 12, pp. 240–251, 2016.

[28]	M. Kubiak, W. Piekarska, and R. Parkitny, “Theoretical study on thermal and structural phenomena in thin elements heated by a laser beam,” Arch. Mech., vol. 67, no. 1, pp. 3–24, 2015.

[29]	A. Simchi, “Direct laser sintering of metal powders: Mechanism, kinetics and microstructural features,” Mater. Sci. Eng. A, vol. 428, no. 1–2, pp. 148–158, 2006.

[30]	D. Buchbinder, G. Schilling, W. Meiners, N. Pirch, and K. Wissenbach, “Investigation to reduce warpage due to preheating in the production of aluminum components using SLM,” RTejournal, pp. 1–16, 2011.

[31]	B. Ahmad, S. O. van der Veen, M. E. Fitzpatrick, and H. Guo, “Residual stress evaluation in selective-laser-melting additively manufactured titanium (Ti-6Al-4V) and inconel 718 using the contour method and numerical simulation,” Addit. Manuf., vol. 22, no. May, pp. 571–582, 2018.

[32]	T. Mukherjee, W. Zhang, and T. DebRoy, “An improved prediction of residual stresses and distortion in additive manufacturing,” Comput. Mater. Sci., vol. 126, pp. 360–372, 2017.

[33]	Jaroslav Menčík, “Latin Hypercube Sampling,” in Concise Reliability for Engineers, vol. i, IntechOpen, 2016, pp. 118–119.

# Appendix

Table 8-1 - Porous material properties computed with NASA’s MAC/GMC from Table 3-1

| Material | T (°C) | Vf | E (MPa) | υ | ρ kgm3 | k Wm2∘C | C JkgoC | α 1°C | Sy (MPa) | εp,1 | S1 (MPa) | εp,2 | S2 (MPa) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Powder | 20 | 0.66 | 7,550 | 0.190 | 1,780 | 3.63 | 270 | 1.26E-5 | 324 | 0.032 | 270 | 0.088 | 298 |
|  |  | 0.81 | 7,550 | 0.225 | 2,180 | 5.10 | 332 | 1.26E-5 | 327 | 0.032 | 380 | 0.088 | 419 |
|  |  | 0.95 | 7,550 | 0.270 | 2,560 | 7.33 | 389 | 1.26E-5 | 469 | 0.032 | 546 | 0.088 | 602 |
|  |  | 0.999 | 7,550 | 0.310 | 2,690 | 9.69 | 410 | 1.26E-5 | 621 | 0.032 | 722 | 0.088 | 796 |
|  | 200 | 0.66 | 21,328 | 0.184 | 1,780 | 4.63 | 301 | 1.31E-5 | 227 | 0.032 | 273 | 0.088 | 273 |
|  |  | 0.81 | 27,707 | 0.218 | 2,180 | 6.50 | 369 | 1.31E-5 | 317 | 0.075 | 382 | 0.244 | 455 |
|  |  | 0.95 | 37,316 | 0.262 | 2,560 | 6.50 | 433 | 1.31E-5 | 456 | 0.075 | 550 | 0.244 | 655 |
|  |  | 0.999 | 47,677 | 0.285 | 2,630 | 9.35 | 456 | 1.31E-5 | 540 | 0.075 | 652 | 0.244 | 776 |
|  | 400 | 0.66 | 36,637 | 0.183 | 1,780 | 5.67 | 337 | 1.36E-5 | 182 | 0.111 | 232 | 0.236 | 262 |
|  |  | 0.81 | 50,104 | 0.217 | 2,180 | 7.96 | 414 | 1.36E-5 | 256 | 0.111 | 325 | 0.236 | 368 |
|  |  | 0.95 | 70,389 | 0.260 | 2,560 | 11.44 | 485 | 1.36E-5 | 367 | 0.111 | 468 | 0.236 | 529 |
|  |  | 0.999 | 92,183 | 0.299 | 2,690 | 15.13 | 510 | 1.36E-5 | 486 | 0.111 | 618 | 0.236 | 700 |
|  | 700 | 0.66 | 59,600 | 0.188 | 1,780 | 7.33 | 383 | 1.50E-5 | 186 | 0.099 | 255 | 0.155 | 267 |
|  |  | 0.81 | 83,700 | 0.223 | 2,180 | 10.30 | 470 | 1.50E-5 | 261 | 0.099 | 359 | 0.155 | 375 |
|  |  | 0.95 | 120,000 | 0.267 | 2,560 | 14.81 | 551 | 1.50E-5 | 375 | 0.099 | 516 | 0.155 | 540 |
|  |  | 0.999 | 159,142 | 0.307 | 2,690 | 19.58 | 579 | 1.50E-5 | 496 | 0.099 | 682 | 0.155 | 714 |

Table 8-2 – Continuation of Table 8-1

| Sintered | 20 | 0.66 | 75,500 | 0.190 | 1,780 | 3.63 | 270 | 1.26E-5 | 324 | 0.032 | 270 | 0.088 | 298 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 0.81 | 106,000 | 0.225 | 2,180 | 5.10 | 332 | 1.26E-5 | 327 | 0.032 | 380 | 0.088 | 419 |
|  |  | 0.95 | 152,514 | 0.270 | 2,560 | 7.33 | 389 | 1.26E-5 | 469 | 0.032 | 546 | 0.088 | 602 |
|  |  | 0.999 | 201,646 | 0.310 | 2,690 | 9.69 | 410 | 1.26E-5 | 621 | 0.032 | 722 | 0.088 | 796 |
|  | 200 | 0.66 | 71,400 | 0.184 | 1,780 | 4.63 | 301 | 1.31E-5 | 227 | 0.032 | 273 | 0.088 | 273 |
|  |  | 0.81 | 100,000 | 0.218 | 2,180 | 6.50 | 369 | 1.31E-5 | 317 | 0.075 | 382 | 0.244 | 455 |
|  |  | 0.95 | 144,290 | 0.262 | 2,560 | 6.50 | 433 | 1.31E-5 | 456 | 0.075 | 550 | 0.244 | 655 |
|  |  | 0.999 | 190,773 | 0.285 | 2,690 | 9.35 | 456 | 1.31E-5 | 540 | 0.075 | 652 | 0.244 | 776 |
|  | 400 | 0.66 | 67,000 | 0.183 | 1,780 | 5.67 | 337 | 1.36E-5 | 182 | 0.111 | 232 | 0.236 | 262 |
|  |  | 0.81 | 94,100 | 0.217 | 2,180 | 7.96 | 414 | 1.36E-5 | 256 | 0.111 | 325 | 0.236 | 368 |
|  |  | 0.95 | 135,319 | 0.260 | 2,560 | 11.44 | 485 | 1.36E-5 | 367 | 0.111 | 468 | 0.2360 | 529 |
|  |  | 0.999 | 178,911 | 0.299 | 2,690 | 15.13 | 510 | 1.36E-5 | 486 | 0.111 | 618 | 0.236 | 700 |
|  | 700 | 0.66 | 59,600 | 0.188 | 1,780 | 7.33 | 383 | 1.50E-5 | 186 | 0.099 | 255 | 0.155 | 267 |
|  |  | 0.81 | 83,700 | 0.223 | 2,180 | 10.30 | 470 | 1.50E-5 | 261 | 0.099 | 359 | 0.155 | 375 |
|  |  | 0.95 | 120,000 | 0.267 | 2,560 | 14.81 | 551 | 1.50E-5 | 375 | 0.099 | 516 | 0.155 | 540 |
|  |  | 0.999 | 159,142 | 0.307 | 2,690 | 19.58 | 579 | 1.50E-5 | 496 | 0.099 | 682 | 0.155 | 714 |

Table 8-3 - Linear regression results, Chapter 5, MPa - mm units

|  |  | Linear |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Before Stress Relief |  |  |  | After Stress Relief |  |  |  |
| Max Svm |  | Coefficient | Std. Error | t-value | Pr(>¦t¦) | Coefficient | Std. Error | t-value | Pr(>¦t¦) |
|  | (Intercept) | 1228.154 | 119.617 | 10.267 | 2.03E-09 | 1003.286 | 172.327 | 5.822 | 1.07E-05 |
|  | Thickness | -44.345 | 15.568 | -2.848 | 0.009931 | -22.178 | 22.428 | -0.989 | 0.33455 |
|  | Radius | -49.815 | 11.015 | -4.522 | 0.000208 | -48.936 | 15.869 | -3.084 | 0.00586 |
|  | Length | 1.298 | 3.355 | 0.387 | 0.702959 | 4.767 | 4.834 | 0.986 | 0.33582 |
|  | R-squared | 63.28% |  |  |  | 0.4599 |  |  |  |
|  | P-value | 3.44E-05 |  |  |  | 0.005572 |  |  |  |
| Max. Udia | (Intercept) | 0.0071431 | 0.009366 | 0.763 | 4.55E-01 | 0.0051935 | 0.007025 | 0.739 | 4.68E-01 |
|  | Thickness | -0.000135 | 0.001219 | -0.111 | 0.913 | -0.0008699 | 0.000914 | -0.951 | 0.3527 |
|  | Radius | 0.0003842 | 0.0008625 | 0.445 | 0.661 | 0.0035903 | 0.000647 | 5.55 | 1.97E-05 |
|  | Length | 0.0001082 | 0.0002627 | 0.412 | 0.685 | -0.0003726 | 0.000197 | -1.891 | 0.0732 |
|  | R-squared | 1.42% |  |  |  | 0.6897 |  |  |  |
|  | P value | 0.9613 |  |  |  | 2.59E-05 |  |  |  |
| Avg. Svm | (Intercept) | 259.181 | 52.6277 | 4.925 | 8.17E-05 | 137.193 | 38.844 | 3.532 | 2.09E-03 |
|  | Thickness | 0.7344 | 6.8495 | 0.107 | 0.915679 | -3.619 | 5.056 | -0.716 | 0.48237 |
|  | Radius | -3.4792 | 4.8463 | -0.718 | 0.481122 | -1.723 | 3.577 | -0.482 | 0.63521 |
|  | Length | -7.0895 | 1.4763 | -4.802 | 0.000108 | -1.746 | 1.09 | -1.602 | 0.12477 |
|  | R-squared | 54.30% |  |  |  | 0.153 |  |  |  |
|  | P-value | 0.001122 |  |  |  | 0.3338 |  |  |  |
| Avg. Umag | (Intercept) | -0.0008025 | 0.003716 | -0.216 | 8.31E-01 | 0.002199 | 0.003548 | 0.62 | 5.43E-01 |
|  | Thickness | -0.000373 | 0.0004837 | -0.771 | 0.4496 | -0.0004274 | 0.000462 | -0.926 | 0.3657 |
|  | Radius | 0.000672 | 0.0003422 | 1.964 | 0.0636 | 0.002071 | 0.000327 | 6.338 | 3.48E-06 |
|  | Length | 0.00005566 | 0.0001042 | 0.534 | 0.5993 | -0.0003281 | 9.95E-05 | -3.297 | 0.0036 |
|  | R-squared | 16.27% |  |  |  | 0.7763 |  |  |  |
|  | P-value | 0.3033 |  |  |  | 1.04E-06 |  |  |  |

Table 8-4 - Quadratic regression results, Chapter 5, MPa - mm units

|  |  | Before Stress Relief |  |  |  | After Stress Relief |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Max Svm |  | Coefficient | Std. Error | t-value | Pr(>¦t¦) | Coefficient | Std. Error | t-value | Pr(>¦t¦) |
|  | (Intercept) | 609.083 | 16.501 | 36.913 | 2.37E-15 | 514.61 | 12.53 | 41.085 | 5.36E-16 |
|  | Radius | -345.621 | 95.236 | -3.629 | 0.00274 | -374.98 | 72.29 | -5.187 | 0.000138 |
|  | Radius^2 | -8.446 | 100.901 | -0.084 | 0.93447 | 106.37 | 76.59 | 1.389 | 0.186594 |
|  | Thickness | -170.954 | 89.578 | -1.908 | 0.07705 | -69.74 | 68 | -1.026 | 0.322457 |
|  | Thickness* Radius | 56.509 | 518.138 | 0.109 | 0.9147 | 339.27 | 393.31 | 0.863 | 0.402899 |
|  | Thickness^2 | -120.106 | 76.233 | -1.576 | 0.13746 | -335.94 | 57.87 | -5.805 | 4.56E-05 |
|  | Length | 31.889 | 82.385 | 0.387 | 0.70452 | 86.85 | 62.54 | 1.389 | 0.18661 |
|  | Length* Radius | -74.3 | 460.981 | -0.161 | 0.87426 | 533.17 | 349.93 | 1.524 | 0.149859 |
|  | Length* Thickness | -123.71 | 568.108 | -0.218 | 0.83076 | 715.86 | 431.25 | 1.66 | 0.119142 |
|  | Length^2 | -53.76 | 77.721 | -0.692 | 0.50043 | -166.45 | 59 | -2.821 | 0.013598 |
|  | R-squared | 74.0% |  |  |  | 87.8% |  |  |  |
|  | P-value | 0.006667 |  |  |  | 5.55E-05 |  |  |  |
| Max. Udia | (Intercept) | 0.0119062 | 0.0012647 | 9.414 | 1.96E-07 | 0.0318141 | 0.000867 | 36.706 | 2.56E-15 |
|  | Radius | 0.004514 | 0.0072996 | 0.618 | 0.546 | 0.0227725 | 0.005003 | 4.552 | 0.000452 |
|  | Radius^2 | 0.0083036 | 0.0077337 | 1.074 | 0.301 | 0.0027932 | 0.0053 | 0.527 | 0.606425 |
|  | Thickness | -0.00359 | 0.0068659 | -0.523 | 0.609 | -0.004953 | 0.004705 | -1.053 | 0.310334 |
|  | Thickness* Radius | -0.0290408 | 0.0397136 | -0.731 | 0.477 | -0.0068556 | 0.027216 | -0.252 | 0.804781 |
|  | Thickness^2 | -0.0004888 | 0.005843 | -0.084 | 0.935 | 0.0015943 | 0.004004 | 0.398 | 6.97E-01 |
|  | Length | 0.0054756 | 0.0063146 | 0.867 | 0.4 | -0.0063704 | 0.004327 | -1.472 | 0.163118 |
|  | Length* Radius | -0.0158845 | 0.0353327 | -0.45 | 0.66 | -0.0214015 | 0.024214 | -0.884 | 0.391699 |
|  | Length* Thickness | -0.0137141 | 0.0435436 | -0.315 | 0.757 | -0.0127435 | 0.029841 | -0.427 | 0.675839 |
|  | Length^2 | 0.0020187 | 0.0059571 | 0.339 | 0.74 | 0.0058023 | 0.004082 | 1.421 | 0.177129 |
|  | R-squared | 23.1% |  |  |  | 79.8% |  |  |  |
|  | P-value | 0.8742 |  |  |  | 0.001425 |  |  |  |
| Avg. Svm | (Intercept) | 140.555 | 6.619 | 21.237 | 4.76E-12 | 86.585 | 4.894 | 17.692 | 5.63E-11 |
|  | Radius | -10.371 | 38.2 | -0.271 | 0.78997 | 1.203 | 28.247 | 0.043 | 0.967 |
|  | Radius^2 | 48.861 | 40.472 | 1.207 | 0.24733 | 50.219 | 29.927 | 1.678 | 0.116 |
|  | Thickness | -9.538 | 35.93 | -0.265 | 0.79452 | -24.738 | 26.569 | -0.931 | 0.368 |
|  | Thickness* Radius | -18.305 | 207.828 | -0.088 | 0.93106 | -38.208 | 153.679 | -0.249 | 0.807 |
|  | Thickness^2 | 29.136 | 30.577 | 0.953 | 0.35683 | 16.53 | 22.61 | 0.731 | 4.77E-01 |
|  | Length | -129.034 | 33.045 | -3.905 | 0.00159 | -23.217 | 24.435 | -0.95 | 0.358 |
|  | Length* Radius | -35.501 | 184.902 | -0.192 | 0.8505 | -15.572 | 136.726 | -0.114 | 0.911 |
|  | Length* Thickness | -113.541 | 227.872 | -0.498 | 0.62603 | -26.472 | 168.5 | -0.157 | 0.877 |
|  | Length^2 | 20.85 | 31.175 | 0.669 | 0.5145 | -16.508 | 23.052 | -0.716 | 0.486 |
|  | R-squared | 69.1% |  |  |  | 42.4% |  |  |  |
|  | P-value | 0.01842 |  |  |  | 0.3946 |  |  |  |
| Avg. Umag | (Intercept) | 0.0046787 | 0.0004255 | 10.995 | 2.85E-08 | 0.0161753 | 0.000373 | 43.33 | 2.56E-16 |
|  | Radius | 0.0030901 | 0.002456 | 1.258 | 0.2289 | 0.0119223 | 0.002155 | 5.533 | 7.37E-05 |
|  | Radius^2 | 0.0028217 | 0.0026021 | 1.084 | 0.2965 | 0.0010266 | 0.002283 | 0.45 | 0.6598 |
|  | Thickness | -0.0005108 | 0.0023101 | -0.221 | 0.8282 | -0.001487 | 0.002027 | -0.734 | 0.4752 |
|  | Thickness* Radius | 0.007655 | 0.0133619 | 0.573 | 0.5758 | 0.002278 | 0.011722 | 0.194 | 0.8487 |
|  | Thickness^2 | 0.0008576 | 0.0019659 | 0.436 | 0.6693 | 0.0014702 | 0.001725 | 0.852 | 4.08E-01 |
|  | Length | 0.0008711 | 0.0021246 | 0.41 | 0.688 | -0.0068737 | 0.001864 | -3.688 | 0.00244 |
|  | Length* Radius | -0.02108 | 0.011888 | -1.773 | 0.0979 | -0.0244181 | 0.010429 | -2.341 | 0.03453 |
|  | Length* Thickness | 0.0077598 | 0.0146506 | 0.53 | 0.6046 | 0.0027223 | 0.012853 | 0.212 | 0.83531 |
|  | Length^2 | -0.003236 | 0.0020043 | -1.615 | 0.1287 | 0.001926 | 0.001758 | 1.095 | 0.29184 |
|  | R-squared | 53.0% |  |  |  | 89.4% |  |  |  |
|  | P-value | 0.1668 |  |  |  | 2.18E-05 |  |  |  |